## Slide 1
Weed Control
Srijana Shrestha, Huan Zhang, Lisa DeVetter, and Carol Miles
Washington State University
Soil-Biodegradable Plastic Mulch Professional Training
https://smallfruits.wsu.edu
biodegradablemulch.org
Notes: This presentation provides information on the use of soil-biodegradable mulch (BDM) for weed control, effect of different colors of plastic mulch on light and weed control, how percent soil exposure (PSE) relates to weed growth, and comparison between polyethylene (PE) mulch and BDM in terms of weed control and crop yield.

## Slide 2
Crop-weed Competition and Mulch
Weeds compete for:
Nutrients
Water
Light
Polyethylene (PE) mulch is good at controlling weeds
What about BDMs?
https://smallfruits.wsu.edu
biodegradablemulch.org
Notes: Weed control is the primary function of mulch. Weeds compete with the main crop for nutrients, water, and light which causes adverse effects on crop growth. PE mulch is very effective for weed control, but what about BDMs?

## Slide 3
Light and Weed Control
https://smallfruits.wsu.edu
biodegradablemulch.org
Comparison of the effect of different colors of plastic on soil temperature, light and weed control
Angima, 2009; Penn State Extension, 2015; Sanders, 2001
Notes: This table (Table 1) shows the comparison of the effect of different colors of plastic on light and weed control. For example, black plastic mulch has low light reflectivity, high light absorptivity and low light transmission, thus it provides excellent weed suppression. Clear plastic mulch provides poor weed suppression because of high light transmission. Mulches that selectively filter out light in the photosynthetically active radiation (PAR) range are called infrared transmitting (IRT) mulches. IRT mulches tend to transmit high percentages of light at longer wavelengths (>900 nm) and allow for greater soil warming while reducing light available for weed growth.

## Slide 4
Percent Soil Exposure (PSE) in Pumpkin
Zhang et al., 2020
Black AMX-01 WeedGuardPlus Black Film Organic Clear Organix Black Organix Black polyethylene Clear polyethylene
254 µm 240µm 15.2 µm 17.8 µm 15.2 µm 25.4 µm 25.4 µm
2018
2019
PSE during pumpkin growing season in Mount Vernon, WA; 0% = completely intact, 100% = fully deteriorated, ratings in 1% increments up to 20%, and 5% increments thereafter; error bar is ± one standard error of the mean. 25.4 µm = 1 mil.
https://smallfruits.wsu.edu
biodegradablemulch.org
Growing season = 16 wk
Notes: The graphs (Fig. 1) show the percent soil exposure (PSE) during the pumpkin growing season of about 16 weeks in Mount Vernon, WA in 2018 and 2019. When the mulch deteriorates, the soil gets exposed and there is potential for weed growth. 0% PSE denotes completely intact mulch while 100% PSE denotes completely deteriorated mulch. Ratings were in 1% increments up to 20% PSE, and in 5% increments thereafter. PSE was highest for Clear Organix mulch in both years (63% in 2018, and 74% in 2019). All other BDMs reached a maximum of 10% PSE in 2018 and 15% in 2019.

## Slide 5
Weed number per m2 in plots with ‘Cinnamon Girl’ pie pumpkin grown with clear and black polyethylene (CPE and BPE) and soil-biodegradable mulch treatments [AMX-01 (AMX), WeedGuardPlus (WGP), Black Film Organic (BFO), Clear Organix (COX), and Black Organix (BOX)] in 2018 and 2019.
Weed Populations under Mulch in Pumpkin
https://smallfruits.wsu.edu
biodegradablemulch.org
Zhang et al., 2020
Notes: This table (Table 2) shows the weed population per m2 under mulch at three different times, early season, mid-season, and late season in 2018 and 2019. Weed number was low for all the treatments except Clear Organix mulch (COX) in 2018 and 2019 plus Clear polyethylene mulch (CPE) in 2019. Weed growth occurred beneath the clear plastic mulch treatments because they allowed light transmission. However, weeds continued to grow in Clear Organix mulch (COX) due to splitting early in the season. The higher weed number in Clear polyethylene mulch (CPE) in 2019 was likely due to higher soil moisture than in 2018. Weed growth in late season was due to mulch deterioration. Other BDM treatments provided effective weed control similar to black polyethylene mulch.

## Slide 6
July 2019
(6 weeks after transplanting)
Zhang et al., 2020
Oct. 2019
(18 weeks after transplanting)
Pumpkin
BDM (BOX 0.6 mil)
PE (1 mil)
Notes: This (Fig. 2) is how Black Organix mulch (BOX) and Black polyethylene mulch (BPE) look in July 2019 and October 2019 in pumpkin. They are both intact with essentially no weeds.

## Slide 7
NS: nonsignificant * P ≤ 0.05
PSE of mulch (0.5 = 12.7 μm thickness, 0.6 = 15.2 μm thickness) in raspberry production in Lynden, WA; 0% = completely intact, 100% = fully deteriorated, ratings in 1% increments up to 20%, and 5% increments thereafter; error bar is ± one standard error of the mean.
Zhang et al., 2020
Percent Soil Exposure (PSE) in Raspberry
16 wk
Notes: This graph (Fig. 3) represents the PSE for a period of 1 year during raspberry production in Lynden, WA. At 16 weeks, BDM deterioration was about 8% on average, similar as with pumpkin. But 1 year after application, all the black plastic BDMs reached about 90% PSE while PE mulch remained almost completely intact.

## Slide 8
BDM (BASF 0.6 mil)
PE (1 mil)
June 2017
(3 weeks after transplanting)
Zhang et al., 2020
Dec. 2017
(28 weeks after transplanting)
Raspberry
Notes: This (Fig. 4) is how BDM and PE mulch look in June 2017 and December 2017 in raspberry. BDM is deteriorated and has weed growth while PE mulch is intact with no weeds.

## Slide 9
Crop Production with BDMs
1 + BDM performed better; = BDM performed equivalent to; - BDM did not perform as well; empty cell not measured.
2 Reports provide variable results.
https://smallfruits.wsu.edu
biodegradablemulch.org
Adapted from Cowan and Miles, 2018
 | Yield |  | Weed Control
Crop | vs. Bare ground | vs. PE | vs. PE
Broccoli | +1 |  | 
Cucumber | + | = | =
Eggplant | + | = | -
Lettuce |  | -=2 | 
Melon | + | += | ≅
Pepper | = | = | -
Pumpkin |  | = | =
Raspberry | + | = | =
Strawberry | + | -=+2 | -
Sweet Corn | + | -= | -
Sweet Potato | + | += | +
Tomato | + | = | ≅
Zucchini |  | = | 
Notes: This table (Table 3) represents crop production with BDMs. In the same pumpkin study, fruit yield and weed control were comparable between black plastic BDMs and PE mulch. Yield is greater compared with bare ground and essentially the same as with PE mulch in other crops. Weed control varies between BDM and PE mulch depending on crop and location. BDMs tend to deteriorate after 12 weeks and while this leads to some weed growth, it tends to be late enough that it has little impact on yield. Thus overall, BDM has shown comparable horticultural benefits with PE mulch in research results.

## Slide 10
Resources
https://smallfruits.wsu.edu
biodegradablemulch.org
DeVetter, L.W., H. Zhang, S. Ghimire, S. Watkinson, and C.A. Miles. 2017. Plastic biodegradable mulches reduce weeds and promote crop growth in day-neutral strawberry in western Washington. HortScience 52:1700-1706.
Ghimire, S., E. Scheenstra, and C.A. Miles. 2020. Soil-biodegradable mulches for growth and yield of sweet corn in Mediterranean-type climate. HortScience 55:317-325.
Ghimire, S., A.L. Wszelaki, J.C. Moore, D.A. Inglis, and C. Miles. 2018. The use of biodegradable mulches in pie pumpkin crop production in two diverse climates. HortScience 53:288-294. https://doi.org/10.21273/HORTSCI12630-17.
Moore, J. C. and Wszelaki, A. L. (2019). The use of biodegradable mulches in pepper production in the Southeastern United States. HortScience 54:1031–1038.
Video – 2019 SFC Raspberry Talk (start at 10 minutes) https://www.youtube.com/watch?v=W5J-P_32MGQ&feature=youtu.be
Zhang, H., L.W. DeVetter, E. Scheenstra, and C. Miles. 2020. Weed pressure, yield, and adhesion of soil-biodegradable mulches with pie pumpkin (Cucurbita pepo). HortScience 55: 1014-1021 https://doi.org/10.21273/HORTSCI15017-20