Project ID: 2022-MST-04

Comprehensive Assessment of Innovative Paving Materials Through Long-Term Pavement Performance (LTPP) Database and State Specifications

Final Report

By

Jenny Liu, Ph. D., P.E.

James A. Heidman Professor

Missouri University of Science and Technology

Seyed Alireza Ghanoon

Ph.D. student

Missouri University of Science and Technology

for

National University Transportation Center TriDurLE

Department of Civil & Environmental Engineering

405 Spokane Street PO Box 642910

Washington State University, Pullman, WA 99164-2910

August 2024

# Acknowledgements

The authors extend their gratitude to the National Center for Transportation Infrastructure Durability & Life-Extension for funding this research.

# Disclaimer

The contents of this report reflect the views of the authors, who are responsible for the facts and the accuracy of the information presented. This document is disseminated under the sponsorship of the Department of Transportation, University Transportation Centers Program, in the interest of information exchange. The U.S. Government assumes no liability for the contents or use thereof.

# Table of Contents

Acknowledgements	i

Disclaimer	i

Table of Contents	ii

List of Figures	iv

List of Tables	v

Executive Summary	vi

Chapter 1	Introduction	1

1.1	Problem Statement	1

1.2	Objectives	3

1.3	Methodology	3

1.4	Organization of the Report	4

Chapter 2	Definition and Background	6

2.1 Introduction	6

2.2 Designation	7

2.3 Sample Preparation and Testing Procedures	10

2.4 Performance Characteristics and Benefits	10

2.5 Performance-Driven Criteria	11

2.6 Usage and Application	12

Chapter 3	Specifications	17

3.1 Introduction	17

3.2 Northeastern USA	17

3.3 South/Southeastern USA	20

3.4 Midwest USA	22

3.5 Western USA	26

Chapter 4	LTPP Database	29

4.1 Introduction	29

4.2 Standard Data Release (SDR)	30

4.2.1 Material Test File	31

4.2.2 Inventory File	35

4.3. Analysis-Ready Materials Dataset (ARMAD)	40

Chapter 5	Discussions	42

5.1 Overview	42

5.2 Comparison of DOT Specifications for Asphalt Binder Modifications	42

5.2.1 Regional Influences on Asphalt Binder Specifications	43

5.2.2 Analysis of DOT Specification Variations	45

5.3 Assessment of LTPP Database Coverage on Modified Binders	46

5.3.1 Data Sources for Modified Binders	47

5.3.2 Coverage and Limitations	47

5.3.3 Implications for Research and Pavement Performance	48

5.3.4 Identifying Gaps in Data: Challenges in Evaluating Modified Binders	48

Chapter 6. Conclusions and Recommendations	50

6.1 Conclusion	50

6.2 Recommendations	51

References	52

# List of Figures

Figure 2.1. Diagram of typical asphalt binder behavior throughout the pavement lifecycle	8

Figure 2.2. Comparative performance of asphalt binders over time based on PSI	9

Figure 2.3. Pavement design for NCAT sections N7 and S9.	10

Figure 2.4. Map showing survey response status of U.S. and Canadian provincial agencies	14

Figure 2.5. U.S. map displaying agency experience with HP asphalt concrete mixtures	15

Figure 2.6. Experience duration with HP asphalt concrete mixtures across U.S. agencies	16

# List of Tables

Table 2.1. Summary of agency specifications for HP asphalt binders and mixtures	12

Table 3.1. PG binders in the Northeastern USA	18

Table 3.2. PG binders in the South/Southeastern USA	20

Table 3.3. PG binders in the Midwest USA	22

Table 3.4. PG binders in the Western USA	26

Table 4.1. Experiment codes and descriptions for LTPP projects	31

Table 4.2. Sections classified under “AC Overlay with Modified Asphalt Cement on AC Pavement, No Milling”	32

Table 4.3. Sections classified under “AC Overlay with Modified Asphalt Cement on PCC Pavement, with CPR or No Pretreatment”	34

Table 4.4. Content of “INV_PMA_ASPHALT” table	36

Table 4.5. Different modifier in LTPP database	37

Table 4.6. Asphalt grade codes in LTPP database	38

Table 4.7. Pavement sections utilizing modified binders identified in the LTPP database	39

Table 4.8. Content of analysis-ready materials dataset (ARMAD)	40

Table 4.9. Analysis of asphalt cement in ARMAD	41

# Executive Summary

Over the last three decades, pavement engineers have collected a substantial amount of construction and field data, one of the most notable achievements being the creation and ongoing development of the Long-Term Pavement Performance (LTPP) database. This database encompasses detailed information on 2,581 pavement sections across various U.S. states, territories, and Canadian provinces, including data on climate, traffic, pavement structure, construction history, and pavement performance. In addition to the LTPP, State Highway Agencies (SHAs) have developed their own Pavement Management System (PMS) databases, which store design information, construction history, and field performance data crucial for making informed decisions in pavement construction and management.

Despite the vast amount of data available, there has been insufficient research focused on leveraging these resources to develop predictive models for innovative paving materials. These materials, which include Stone Matrix Asphalt (SMA), warm mix asphalt, modified asphalt binders, and environmentally friendly options that incorporate recycled materials such as Recycled Asphalt Pavement (RAP), Recycled Asphalt Shingles (RAS), and waste plastic, have been increasingly adopted across the United States. However, the systematic organization and analysis of data related to these materials remain underdeveloped.

The primary objective of this project is to perform a comprehensive data mining effort on the existing pavement data, particularly focusing on innovative paving materials. The research seeks to collect, organize, and analyze data from the LTPP database to develop predictive models that can assess pavement performance, material properties, and the effects of traffic and maintenance. The ultimate goal is to provide highway agencies with the tools needed to improve pavement design, maintenance, and management practices, thereby enhancing the durability and life-extension of transportation infrastructure.

This project employed several methodologies to identify the use of modified binders within the LTPP database. The analysis involved using direct information from the database and reviewing state specifications. The findings revealed limitations in data availability and consistency, underscoring the need for improved data management practices within the LTPP framework.

A detailed review of the specifications for Performance Grade (PG) binders across different regions of the United States was conducted to understand the regional variations and their impact on pavement performance. The report highlighted how different states employ various PG binders to optimize performance, durability, and cost-effectiveness. For instance, the Northeastern states face significant temperature variations and often use binders like PG 64S-22 and PG 64E-22 for standard and high-performance applications, respectively. In contrast, the Southern states, which experience high temperatures and humidity, often utilize PG 76-22 PMA (Polymer Modified Asphalt) for areas requiring greater temperature resistance.

In the Midwest and Western regions, the diversity of PG binders is influenced by climatic conditions and performance needs, with modified binders such as PG 64-22 and PG 70-28 being common in the Midwest, and rubber-modified binders being prevalent in Western states like Nevada and New Mexico for enhanced performance in extreme conditions. The report also detailed the application and experience of modified binders across various U.S. states and Canadian provinces, revealing a growing interest and confidence in the potential benefits of these materials.

The research further delved into the LTPP database, utilizing both the Standard Data Release (SDR) and Analysis-Ready Materials Dataset (ARMAD) methods to identify pavement sections with modified binders and evaluate their performance. The analysis of these datasets has provided valuable insights into the use of modified binders in asphalt pavements across North America. The research also highlighted gaps in data coverage and the challenges of evaluating these binders due to inconsistencies in data collection and reporting.

The findings of this project emphasized the importance of ongoing research and collaboration among transportation agencies to optimize the use of modified binders in pavement engineering. The recommendations include further standardization of data collection practices within the LTPP framework and continued exploration of innovative materials to ensure the long-term sustainability of pavement infrastructure.

In conclusion, this project provided a comprehensive evaluation and prediction of the performance of innovative paving materials through systematic data mining of the LTPP and PMS databases. The outcomes of this research will serve as a valuable resource for highway agencies, supporting their efforts to enhance the design, maintenance, and management of pavement infrastructure, ultimately leading to more durable and sustainable transportation systems.

# Introduction

## Problem Statement

Over the past three decades, pavement engineers have amassed a considerable amount of construction and field data, culminating in one of the most significant achievements in the field: the establishment and continuous development of the Long-Term Pavement Performance (LTPP) database. This extensive database houses detailed information on 2,581 pavement sections across 90 U.S. states, territories, and Canadian provinces. The LTPP database is a rich resource, containing comprehensive data on various critical factors, including climate conditions, traffic loads, pavement structures, construction histories, and the performance of these pavements over time. Such an extensive compilation of data has provided invaluable insights into the long-term behavior of pavement materials and structures under diverse conditions.

In parallel to the LTPP, local State Highway Agencies (SHAs) have been proactive in collecting their own sets of data, focusing on design information, construction histories, and field performance outcomes to build their Pavement Management System (PMS) databases. These PMS databases have become instrumental in guiding pavement construction and management decisions at the state level. They allow agencies to monitor pavement conditions, predict maintenance needs, and optimize the allocation of resources to ensure the longevity and safety of road networks. Recognizing the strategic importance of data-driven decision-making, the Federal Highway Administration (FHWA) has highlighted asset management, including inspection, maintenance, and emergency response for urban infrastructure, as a key area for future development. This recognition underscores the growing importance of comprehensive data collection and analysis in the effective management of the nation's infrastructure (FHWA 2018).

In recent years, the wealth of data housed within these databases has prompted researchers to apply advanced data mining techniques and machine learning algorithms to develop predictive models for pavement performance. For instance, in 2022, the research team behind this proposal extracted 2,699 data points from the LTPP database and successfully developed a ThunderGBM-based ensemble learning model to predict pavement rideability deterioration (Song et al. 2022). This model represents a significant step forward in leveraging data-driven intelligence to anticipate pavement issues before they manifest. Similarly, other researchers have applied artificial intelligence technologies to forecast pavement distress, with notable studies by Ziari et al. (2015), Kaya et al. (2020), and Marcelino et al. (2021) contributing to the growing body of knowledge in this area. However, these studies have predominantly focused on conventional hot mix asphalt (HMA) materials, which limits the applicability of the developed models to these traditional materials.

Since the early 2000s, there has been a concerted effort among pavement engineers to explore and implement new asphalt mixtures that are both more durable and sustainable than conventional HMAs. These efforts have led to the deployment of various innovative materials across numerous states. For example, Stone Matrix Asphalt (SMA), characterized by its gap-graded aggregate skeleton and high binder content, has been extensively used on heavily trafficked highways (Celaya and Haddock 2006). Beyond the use of different aggregate structures, a variety of additives and modifiers have been introduced into asphalt binders to improve the compatibility and performance of these mixtures. Warm mix asphalt and highly modified asphalt binder (HiMA), the latter typically containing more than 5% modifier by weight, are examples of these advanced materials (Liu 2010, Liu and Liu 2019). In response to growing environmental concerns, there has also been an increased focus on incorporating recycled materials into asphalt mixtures. This includes the use of recycled asphalt pavement (RAP), recycled asphalt shingles (RAS), and waste plastic, which not only improve the sustainability of paving materials but also contribute to waste reduction efforts.

As these innovative materials are implemented, the corresponding construction and performance data have been systematically added to both the LTPP and state PMS databases. For example, in 2021, the Missouri Department of Transportation (MoDOT) collected performance data from test sections containing HMAs modified with ground tire rubber and varying contents of waste plastic (Rath et al. 2023). Despite the collection of such valuable data, there has been a noticeable lack of systematic efforts to organize this information and develop performance prediction models tailored to these innovative paving materials. This gap in research is particularly concerning given the growing adoption of these materials and the need to understand their long-term performance.

This study proposed to address this gap by conducting systematic data mining on the application of innovative paving materials, utilizing both the LTPP and local state PMS databases. The research team created a comprehensive database that includes detailed design, construction, and performance data for these innovative mixtures. By doing so, the study aims to provide an insight that will aid in the selection, design, and management of more durable and sustainable pavement materials, ultimately contributing to the advancement of pavement engineering and infrastructure management.

## Objectives

The primary objective of this study is to conduct a comprehensive evaluation of innovative paving materials using data from the LTPP database. The research aims to systematically identify, collect, organize, and analyze data related to the use of modified asphalt binders, focusing on their performance characteristics, applications, and regional variations across different states. By cross-referencing the LTPP data with state-level specifications, the study seeks to provide a clearer understanding of the factors that influence the performance and durability of modified binders in real-world conditions. This includes evaluating the impact of traffic loads, climatic conditions, and material composition on pavement life and effectiveness. Furthermore, the research will emphasize the cost-effectiveness and environmental benefits of using modified binders, particularly in enhancing pavement longevity and reducing maintenance needs. In addition, recommendations will be made to improve the consistency and reliability of data collection and reporting practices within the LTPP framework, facilitating more informed decision-making in future research and practical applications.

## Methodology

To accurately identify the use of modified binders within the LTPP database, the following methods were employed:

- Direct Information Retrieval from the LTPP Database: This method involved extracting specific data related to modified binders directly from the LTPP database. The process required identifying relevant criteria and codes associated with modified binder usage within the dataset. These codes were carefully analyzed to locate pavement sections that utilized modified binders. However, this approach faced challenges due to the potential for incomplete or outdated records within the database. To mitigate these limitations, the research team employed a systematic review of the available data, ensuring that all relevant sections were identified despite the inconsistencies in record-keeping. The thorough cross-referencing of binder-related codes and project details within the LTPP dataset was critical in capturing the extent of modified binder usage across various pavement sections.

- Cross-Referencing with State Specifications and Reports: To complement the information retrieved from the LTPP database, the research included a comprehensive review of state-level specifications. State highway agencies often maintain detailed records specifying the materials and techniques used in their pavement projects, including the types of binders. By cross-referencing these state documents with the LTPP data, the study was able to identify additional instances of modified binder usage that may not have been fully captured in the LTPP database alone. This method also provided insights into regional variations and practices in binder selection, offering a broader perspective on the application and performance of modified binders across different states.

The analysis concluded that a combination of these two methods is necessary to achieve a comprehensive understanding of the use and performance of modified binders in pavement applications. Further efforts to standardize data collection and reporting within the LTPP framework are recommended to enhance the accuracy and utility of the database for future research and practical applications.

The LTPP database provides valuable insights into the use of modified binders in asphalt pavements across North America. However, the limitations identified in data availability and consistency highlight the need for improved data management practices. The findings underscore the importance of ongoing research and collaboration among agencies to better understand and optimize the use of modified binders in pavement engineering.

## Organization of the Report

This report is organized into six chapters, each detailing a specific aspect of the research. Chapter 1 provides an introduction, including the problem statement, objectives, methodology, and the organization of the report. Chapter 2 offers a definition and background, covering the designation, sample preparation, testing procedures, performance characteristics, benefits, and performance-driven criteria of the materials studied. Chapter 3 focuses on specifications, discussing the various Performance Grade (PG) binders and their application across different regions of the United States. Chapter 4 delves into the LTPP database, analyzing the use of modified binders, and the identification of relevant pavement sections. Chapter 5 presents a discussion of the findings, including insights and limitations. Finally, Chapter 6 concludes the report with a summary of the key outcomes and recommendations for practical application and further study.

This study aims to evaluate the performance of modified binders within the LTPP database, focusing on their impact on pavement performance across varying environmental and traffic conditions. While modified binders are central to this research, they are also representative of a broader category of innovative paving materials that are increasingly being adopted in modern pavement construction. These materials, including RAP, RAS, and warm-mix asphalt, share common goals: enhancing pavement durability, reducing environmental impacts, and improving cost-effectiveness.

By selecting modified binders as the focus of this research, the study provides a pathway to understanding the broader implications of innovative materials in pavement performance. The next chapter will delve deeper into the specifics of modified binders, outlining their composition, testing procedures, and performance characteristics. This will establish the technical foundation for assessing their role, not just as individual materials, but as part of the larger effort to innovate and improve sustainable paving practices.

# Definition and Background

## 2.1 Introduction

In line with the objectives introduced in Chapter 1, this chapter focuses on modified binders—one of the most widely studied and applied innovative materials in pavement engineering. Modified binders, including polymer-modified binders (PMB) and highly polymer-modified binders (HPB), have been selected for this study due to their proven ability to improve pavement performance by addressing key issues such as rutting, cracking, and fatigue. However, these binders are not the only innovative solutions available; they represent a larger category of materials, such as RAP, RAS, and other sustainable options, that are being explored and implemented to advance pavement technology.

By understanding the properties and benefits of modified binders, we gain insight into the broader potential of innovative materials to meet the demands of modern infrastructure. This chapter will provide the necessary background on modified binders, setting the stage for a deeper evaluation of their application and potential within the context of sustainable and long-lasting pavement solutions.

Modified asphalt binders have been created using a variety of advanced technologies to improve the properties of traditional asphalt, making them better suited for specific project needs, including different traffic volumes and various climatic conditions (Yang et al. 2013, Sulyman et al. 2014, Li et al. 2017, Habbouche et al. 2020). Over the past 50 years, these improvements have involved adding materials such as polymers, ground tire rubber, chemical agents like acids, and even recycled substances like engine oils. These enhancements are designed to increase the asphalt’s strength, flexibility, resistance to deformation, and overall durability.

Among these innovations, high polymer binders (HPBs) are particularly noteworthy. HPBs are a specialized type of asphalt binder that contain significantly higher levels of polymers (Peng et al. 2019), with Styrene-Butadiene-Styrene (SBS) being one of the most used. The high polymer content in HPBs is intended to greatly enhance the performance of asphalt mixtures. In contrast to standard polymer modified binders, which have lower polymer content, HPBs are specifically engineered to offer superior resistance to rutting, cracking, and other types of pavement deterioration that occur under severe conditions. This makes them especially valuable for use in areas with heavy traffic loads, such as highways and urban streets, as well as regions with extreme temperature variations.

The advantages of HPBs go beyond just durability. These binders help extend the overall lifespan of pavements by preserving their structural integrity and smoothness over longer periods, even when subjected to harsh environmental conditions (Yildirim 2007, Wu et al. 2024). Additionally, the improved flexibility and elasticity of HPBs enable pavements to better absorb and disperse the stresses caused by traffic and temperature fluctuations, thereby reducing the need for frequent and extensive maintenance. However, these benefits come with certain drawbacks, such as higher initial costs and more complicated handling during construction (Bagui et al. 2012, Wang et al. 2017, Almusawi et al. 2023). Despite these challenges, the long-term benefits of HPBs, including lower maintenance costs and extended pavement life, make them an appealing choice for many transportation agencies.

## 2.2 Designation

The resistance of asphalt concrete (AC) mixtures to permanent deformation, such as rutting, typically requires a stiff binder with low binder content, whereas resistance to various forms of cracking (fatigue, top-down, block, and thermal) needs a more flexible binder and higher binder content. The use of modified asphalt binders allows transportation agencies to design balanced mixtures that can effectively resist both types of distresses, ensuring long-term durability by reducing moisture damage and aging susceptibility (Habbouche et al. 2018).

Figure 2.1 illustrates the typical behavior of neat, modified, and ideal asphalt binders across anticipated temperature ranges over their lifespan in a pavement structure, as documented by the Illinois Department of Transportation (2005). Neat asphalt binders are easier to produce and construct but may experience rutting at high temperatures due to their softer nature, fatigue cracking at intermediate temperatures due to lack of flexibility, and thermal cracking at low temperatures due to brittleness. In contrast, modified asphalt binders, although more difficult to produce and requiring higher construction temperatures, offer improved performance by exhibiting less rutting at high temperatures, reduced fatigue cracking at intermediate temperatures, and decreased thermal cracking at low temperatures due to their stronger and more ductile properties. The ideal asphalt binder, which would provide optimal resistance to all three modes of distress, does not currently exist, as achieving a perfect balance across all temperature ranges remains unattainable.

Figure 2.1. Diagram of typical asphalt binder behavior throughout the pavement lifecycle (Habbouche et al. 2018)

Highly modified binders are characterized by their high polymer content, typically ranging from 7.5% by weight of the binder (TWB). This is significantly higher than the standard polymer content in typical polymer-modified asphalts (PMAs), which usually contain around 3% polymer. The increased polymer content results in a dense polymer network within the asphalt, which significantly improves its mechanical properties and resistance to various forms of distress.

The performance characteristics of highly modified binders include enhanced elasticity, improved tensile strength, and greater resistance to temperature fluctuations. These properties make them less susceptible to rutting and cracking, thus extending the service life of pavements. For instance, binders with a polymer content sufficient to produce grades such as PG 76-22 are commonly used in regions with extreme temperature variations or heavy traffic​.

Figure 2.2 illustrates the performance of different asphalt binders over time, measured by the Present Serviceability Index (PSI). It shows that pavements with high performance (HP) highly modified asphalt binders maintain a higher PSI, indicating better condition and durability, compared to those with traditional polymer-modified and non-polymer modified asphalt binders. The HP binders exhibit the least deterioration, suggesting they are more effective in maintaining pavement quality and extending the pavement's service life.

Figure 2.2. Comparative performance of asphalt binders over time based on PSI

Figure 2.3 illustrates the impact of recalibrating the structural coefficient for PMA mixes according to the AASHTO 1993 Guide. PMA mixes generally have a layer coefficient of 0.44. However, some states, such as Alabama, have recalibrated this coefficient to account for the performance benefits of polymer modification. In Alabama, for example, the structural coefficient was increased to 0.54, with a standard deviation of 0.08 for mixes containing 2-3% polymer. This adjustment has resulted in approximately an 18% reduction in the required asphalt concrete (AC) layer thickness for equivalent design traffic and serviceability. Additionally, higher polymer content in modified binders can further increase the AC structural coefficient, enabling further reductions in layer thickness while still maintaining or enhancing pavement performance (Habbouche et al. 2021).

Figure 2.3. Pavement design for NCAT sections N7 and S9.

## 2.3 Sample Preparation and Testing Procedures

The preparation and testing of highly modified binders involve several critical steps to ensure consistent quality and performance. The process begins with heating the binder to a specific temperature to facilitate thorough mixing with the polymer. The mixture is then poured into pre-heated containers, such as aluminum or glass test tubes, and placed in a controlled environment, typically an oven or water bath, at around 163°C (325°F) for a specified duration, usually 48 hours.

After the storage period, the samples are cooled and analyzed for uniformity. One common test is the ring-and-ball softening point test, which measures the temperature at which the binder softens (Zhu et al. 2021). This test is crucial for assessing the distribution of the polymer within the binder and determining its separation tendency. A low difference in softening points between different sections of the sample indicates a well-blended binder with minimal separation.

## 2.4 Performance Characteristics and Benefits

The incorporation of various polymers in asphalt binders leads to a substantial improvement in their overall performance. This enhancement is primarily due to the formation of an elastomeric network within the binder, which imparts a range of advantageous properties to the asphalt mixture:

- Elastic Response: The elastomeric network enables the binder to exhibit a highly elastic response under load. This characteristic is particularly beneficial at elevated service temperatures, where traditional, unmodified binders might behave more like viscous fluids. In such cases, the polymer-modified binder retains its elasticity, helping to maintain the structural integrity of the pavement and reducing the likelihood of rutting and other forms of deformation.

- Improved Adhesion and Tensile Strength: The presence of the elastomeric network also significantly enhances the adhesive properties and tensile strength of the asphalt binder. This improved adhesion ensures a stronger bond between the asphalt binder and the aggregate, leading to a more cohesive and durable pavement structure. The increased tensile strength further helps the binder to resist cracking and deformation, particularly under high traffic loads and in environments with fluctuating temperatures.

- Reduced Temperature Susceptibility: One of the key benefits of the elastomeric network is its ability to reduce the binder’s susceptibility to temperature changes. This results in a more consistent performance across a wider range of temperatures, minimizing the risks associated with thermal expansion and contraction. By maintaining its properties in both hot and cold conditions, the polymer-modified binder helps prevent common temperature-related issues such as thermal cracking in cold weather and rutting in hot weather.

## 2.5 Performance-Driven Criteria

As Table 1 demonstrates, most agencies defined HP binders based on binder-rheology-related parameters and characteristics rather than the percentage of polymer content. There is a strong emphasis on performance-oriented criteria, focusing on how the binders perform under specific conditions rather than their composition alone. High elasticity and recovery are crucial attributes for good pavement performance, particularly under heavy, stress-concentrated, or slow-moving traffic loads. These properties help HP binders withstand severe stress and deformation, making them ideal for challenging traffic and environmental conditions.

Table 2.1. Summary of agency specifications for HP asphalt binders and mixtures (Habbouche et al. 2021)

| Agency | Standard/Test Method | Properties/Comments |
| --- | --- | --- |
| Alabama | AASHTO M 332, AASHTO T 350 | PG 76E-22 reported as PG 88-22, R3.2 ≥ 90% |
| Alaska | AASHTO M 320 and M 332, AASHTO T 350, AASHTO T 315, ATM 420 | PG 64E-40, Jnr, 3.2 < 0.1 kPa-1 and R3.2 ≥ 95% at 64°C, G*.sinδ < 5,000 kPa at 0°C after PAV, Abrasion of HMA by the Prall test, Prall loss < 20 cm3 |
| Florida | AASHTO T 332, AASHTO T 350, AASHTO T 315 | PG 76E-22, Jnr, 3.2 < 0.1 kPa-1 and R3.2 ≥ 90% at 76°C, G*/sinδ ≤ 1,0 kPa and δ < 75° at 76°C on original, G*.sinδ < 5,000 kPa at 26.5°C after PAV |
| Georgia | AASHTO T 332, AASHTO T 350 | PG 76E-22 reported as PG 82-28, Jnr, 3.2 < 0.1 kPa-1 and R3.2 ≥ 90% at 76°C |
| Iowa | AASHTO M 332, AASHTO T 350 | PG 64-34E+ reported as PG 76-34, R3.2 ≥ 90% at 64°C |
| Kentucky | AASHTO M 320 and M 332, AASHTO T 350 | PG 76E-22 reported as PG 82-22, R3.2 ≥ 90% at 76°C |
| Maryland | AASHTO T 332, AASHTO T 350 | PG 76E-28, Jnr, 3.2 < 0.1 kPa-1 and R3.2 ≥ 90% at 76°C |
| Minnesota | AASHTO M 320, AASHTO T 301 | PG 76-34, Re ≥ 90% |
| Missouri | AASHTO T 332, AASHTO T 350 | PG 76E-22, Jnr, 3.2 < 0.1 kPa-1 and R3.2 ≥ 90% at 76°C |
| Newfoundland and Labrador | AASHTO M 320, AASHTO T 301 | PG 64-34, Re ≥ 60% |
| New Hampshire | AASHTO M 320, AASHTO T 301 | PG 76-34, Re ≥ 90% |
| New Jersey | AASHTO T 332, AASHTO T 350 | PG 64E-22, Jnr, 3.2 < 0.3 – 0.5 kPa-1 at 64°C + depends on the applications and mixture requirements |
| New York | AASHTO M 332, AASHTO T 350 | PG 76E-28, Jnr, 3.2 < 0.5 kPa-1 and R3.2 ≥ 55% at 76°C |
| Ohio | AASHTO M 320, OH DOT TM 429 (as AASHTO T 301) | PG 88-22 reported as PG 88-22M, Re ≥ 90% |
| Oklahoma | AASHTO T 332, AASHTO T 350 | PG 76E-28, R3.2 ≥ 95% at 76°C |
| Oregon | AASHTO M 320, AASHTO T 301 | PG 76-28, Re ≥ 90% |
| Tennessee | AASHTO M 332, AASHTO T 350 | PG 76E-28, Jnr, 3.2 < 0.1 kPa-1 and R3.2 ≥ 90% at 76°C |
| Utah | AASHTO M 320, AASHTO T 301 | PG 76-34, Re ≥ 90% |
| Vermont | AASHTO M 320, AASHTO T 301 | PG 76-34, Re ≥ 90% |
| Virginia | AASHTO T 332, AASHTO T 350 | PG 76E-28(HP), Jnr, 3.2 < 0.1 kPa-1 and R3.2 ≥ 90% at 76°C |
| Washington | AASHTO M 320, AASHTO T 301 | PG 76-34, Re ≥ 90% |
| Wisconsin | AASHTO M 332, AASHTO T 350, AASHTO T 315 | PG 58E-34, Jnr, 3.2 < 0.5 kPa-1 and R3.2 ≥ 75% at 58°C, G*.sinδ < 6,000 kPa at 16°C after PAV + depends on the applications and mixture requirements |

## 2.6 Usage and Application

Overall, the use of modified binders in asphalt mixtures offers significant advantages in terms of durability and performance. These binders are particularly suited for applications where high resilience and long-term performance are critical, making them a valuable component in modern pavement design and construction.

Figure 2.4 provides an overview of a survey conducted in September 2019 via email, targeting U.S. states and Canadian provincial agencies. The survey content covered questions on various aspects, including material specifications, usage, design, performance, constructability, quality control, environmental restrictions, research efforts, costs, benefits, and lessons learned. The response rate was nearly 37%, with 23 responses received from 22 U.S. agencies and one Canadian agency. The survey’s significance lies in providing the first comprehensive look at the usage of HP binders and mixtures across North America (Habbouche et al. 2021).

The survey revealed that 11 U.S. agencies, collectively referred to as Group A, have practical experience with HP binders and mixtures. These agencies have implemented these materials in their pavement projects, demonstrating a commitment to exploring advanced asphalt technologies. The states included in Group A are Alabama (AL), Florida (FL), Georgia (GA), Iowa (IA), Maryland (MD), New Jersey (NJ), New York (NY), Ohio (OH), Vermont (VT), Virginia (VA), and Wisconsin (WI). This group represents a diverse geographical distribution, suggesting a wide range of environmental conditions and application scenarios (Habbouche et al. 2021).

Furthermore, this survey illustrated 10 more U.S. agencies, classified as Group B, also have experience with HP binders and mixtures. These agencies have either utilized HP materials or conducted field trials to evaluate their performance. Group B includes the states of Alaska (AK), Kentucky (KY), Minnesota (MN), Michigan (MI), New Hampshire (NH), Oklahoma (OK), Oregon (OR), Tennessee (TN), Utah (UT), and Washington (WA). The inclusion of these states expands the understanding of HP binder usage across different climatic zones and traffic conditions (Habbouche et al. 2021).

Combining Groups A and B, a total of 21 agencies have either used or conducted field trials with HP AC mixtures. This significant number indicates a growing interest and confidence in the potential benefits of HP binders. The survey findings highlight that most of these agencies are located in the eastern United States. This regional concentration may reflect specific regional needs, such as the requirement for materials that can withstand varying temperature extremes and heavy traffic loads, commonly encountered in the eastern part of the country. The data underscores the importance of HP binders in enhancing pavement performance and durability across diverse environments.

Figure 2.4. Map showing survey response status of U.S. and Canadian provincial agencies (Habbouche et al. 2021)

Figure 2.5 illustrates the distribution of U.S. states based on their experience with HP binders and mixtures, as well as their participation in a related survey. States are categorized into four groups: those currently using or having previously used HP materials and responded to the survey (Group A), including Alabama, Florida, Georgia, Iowa, Maryland, New Jersey, New York, Ohio, Vermont, Virginia, and Wisconsin; those using or having used HP materials but did not respond to the survey (Group B), including Alaska, Kentucky, Minnesota, Michigan, New Hampshire, Oklahoma, Oregon, Tennessee, Utah, and Washington; states with no previous experience with HP materials but responded to the survey, like Mississippi; and states with no experience with HP materials and did not respond to the survey. The map reveals a higher concentration of experience and survey participation in the eastern U.S., particularly in the southeast and northeast regions, suggesting these areas may benefit more from the enhanced performance of HP binders. The map also identifies gaps in experience and survey participation, indicating opportunities for targeted research and outreach to promote HP material adoption in these regions (Habbouche et al. 2021).

Figure 2.5. U.S. map displaying agency experience with HP asphalt concrete mixtures (Habbouche et al. 2021)

According to Figure 2.6, Various U.S. states and Newfoundland and Labrador (Canada) have diverse durations of experience with HP binders, with applications tailored to local needs. States with less than 2 years of experience include Wisconsin and Maryland, while those with 2-4 years of experience are Florida, Georgia, Iowa, Vermont, and Virginia. States with more than 4 years of experience are Alabama, New Jersey, New York, and Ohio, with Newfoundland and Labrador having significant experience with high SBS polymer content. Specific applications include using HP binders in Open Graded Friction Course (OGFC) mixtures to resist raveling in Florida, high performance thin lift overlays in Iowa, dense-graded surface mixtures and Stone Matrix Asphalt (SMA) for reflective cracking in Maryland and Virginia, high polymer thin overlay mixtures, binder-rich intermediate and base courses, bridge deck waterproof surface courses, and high reclaimed asphalt pavement mixtures in New Jersey, polymer-modified stress-absorbing membrane interlayers and waterproofing bridge deck hot mix AC overlays in New York, bridge decks and intersections in Ohio, AC pavement interlayers in Wisconsin, and mitigating studded tire abrasion in Alaska and Newfoundland and Labrador. This comprehensive overview demonstrates the effectiveness and versatility of HP binders in enhancing pavement performance and addressing specific local challenges across various regions.

Figure 2.6. Experience duration with HP asphalt concrete mixtures across U.S. agencies

# Specifications

## 3.1 Introduction

Understanding the diversity of PG binders is crucial for several reasons. It allows for optimized performance by ensuring the pavement meets specific demands and conditions, leading to enhanced durability and functionality. Additionally, it promotes economic efficiency by enabling the selection of cost-effective options that still meet performance requirements. Safety and reliability are also improved, as the appropriate use of PG binders results in safer, more dependable pavement surfaces, reducing the likelihood of accidents and maintenance issues. Furthermore, knowledge of PG binders ensures compliance with various regional regulations and standards, avoiding legal complications. Finally, understanding the environmental impact of different binders helps in making environmentally friendly choices, thereby reducing the negative environmental footprint of pavement projects.

The selection and development of PG binders are influenced by several key factors that vary by region. Primarily, climate and weather conditions, including temperature variations and precipitation levels, significantly impact the choice of binder, as different binders perform better under specific temperature ranges and moisture levels. Additionally, traffic load and volume play a crucial role in determining binder performance requirements, with high traffic volumes and heavy loads demanding binders that can withstand greater stress and provide durability to ensure the pavement remains functional and safe over time. Regional specifications for PG binders are developed by considering climatic considerations, traffic patterns and load, local material availability to ensure cost-effectiveness, and historical performance data to understand how binders have performed under similar conditions. State-specific research and innovations further tailor specifications to local needs, while federal and regional guidelines provide a framework for consistency and compliance. Regulatory and environmental policies ensure that the chosen materials meet safety and environmental standards. Together, these factors create a comprehensive approach to developing PG binder specifications that meet the unique needs of each region. Understanding these elements is essential for selecting the most appropriate PG binder for a given pavement project.

## 3.2 Northeastern USA

In the Northeastern United States, PG binders are selected based on the unique climatic conditions and traffic demands of each state, as highlighted in Table 3.1. The region includes states like Connecticut, Maine, Massachusetts, and others, each employing specific binder grades to ensure pavement durability and performance. The Northeast experiences significant temperature fluctuations, necessitating the use of binders like PG 64S-22 for general use and PG 64E-22, which is enhanced with SBS polymers, for more demanding applications. States such as Maine and New York also integrate crumb rubber-modified binders, like PG 58-28 CR, to boost pavement longevity.

Table 3.1. PG binders in the Northeastern USA

| State | PG Binders | Application & Comments |
| --- | --- | --- |
| Connecticut | 64S-22 | Used in standard pavement applications without the need for enhanced performance characteristics. |
|  | 64E-22 | This binder is modified solely with a Styrene-Butadiene-Styrene (SBS) polymer. It is used where higher performance is required. |
| Delaware | 64-22 | Used for tack coat in thin lift maintenance contracts, typically less than 1 1/4 inches thick. |
|  | 64S-22 |  |
|  | 64E-22 | Used in Superpave asphalt mixtures, including various types like Type C, Type B, Type BCBC, and their applications in different forms such as patching and wedge. |
|  | 70-22 |  |
|  | 76-22 |  |
| Maine | 58-28 | General asphalt binder |
|  | 64-28 |  |
|  | Modified Binders | Used where higher performance is required |
| Maryland | 64-22 | Standard asphalt pavement binder. |
|  | 64S-22 |  |
|  | 64E-22 | Open Graded Friction Course (OGFC) for improved skid resistance. |
|  | 64-28 | High traffic volume roads with higher performance requirements. |
|  | 70-28 | Heavy-duty applications like highways and roads with heavy truck traffic. |
|  | WMA | Warm Mix Asphalt applications, environmentally friendly options. |
| Massachusetts | 64-28 | Standard asphalt binder for Hot Mix Asphalt (HMA) mixtures unless specified otherwise. |
|  | 64E-28 | When specified by contract documents for enhanced performance. |
|  | 58-28 CR Modified | Used for modified asphalt with crumb rubber, often for improved durability and performance. |
|  | 64-28 CR Modified |  |
|  | WMA | All HMA must be modified with a WMA additive, ensuring compatibility with various types of modified binders. |
| New Hampshire | In their specifications, they did not directly mention any specific binders but instead used general requirements. |  |
| New Jersey | 58-28 | Low-temperature performance grade binder |
|  | 64-22 | Standard performance grade binder |
|  | 64S-22 |  |
|  | 64E-22 | Enhanced performance grade binder |
| New York | 58E-34 | These PG binders are used for paving applications, and the specific type depends on the performance requirements such as traffic level and climate conditions. |
|  | 64S-22 |  |
|  | 64V-22 |  |
|  | 64H-22 |  |
|  | 64E-22 |  |
| Pennsylvania | 64S-22 | Previous 19.0 mm Binder Course, cold recycled asphalt base course (CRABC). |
|  | 64H-22 | Previous 9.5 mm Wearing Course. |
|  | 64V-22 | Cold recycled asphalt base course (CRABC). |
|  | 64E-22 | Superpave mixes, including enhanced performance mixes. |
|  | 58S-28 | Cold recycled asphalt base course (CRABC). |
|  | 58V-28 |  |
| Rhode Island | 64S-28 | Dense graded hot mix asphalt (HMA) pavements for Classes 4.75, 9.5, 12.5, 19.0, and base courses. |
|  | 64S-22 | Dense graded HMA pavements for Class 19.0 and base courses with less than 15 percent RAP. |
|  | 58S-22 | Dense graded HMA pavements for Class 19.0 and base courses with 15 to 25 percent RAP. |
|  | 64E-28 SBS Modified | All classes designated as "Modified". |
|  | 64E-28 | Friction courses and specific applications. |
|  | 76E-34 | Paver-placed elastomeric surface treatment (PPEST). |
|  | 58-28 | Rubberized asphalt chip sealing, Precoating cover aggregate for rubberized asphalt chip sealing. |
|  | 64-28 | General pavement construction; Precoating cover aggregate for rubberized asphalt chip sealing. |
| Vermont | 58S-28 | General performance-graded asphalt binder |
|  | 58H-28 | High Traffic performance-graded asphalt binder |
|  | 58V-28 | Very high Traffic performance-graded asphalt binder |
|  | 58E-28 | Extremely high Traffic performance-graded asphalt binder |
|  | 58S-34 | Superior low-temperature performance-graded asphalt binder |
|  | 58H-34 | High traffic performance-graded asphalt binder for low temperatures |
|  | 58V-34 | Very High traffic performance-graded asphalt binder for low temperatures |
|  | 58E-34 | Extremely High traffic performance-graded asphalt binder for low temperatures |
| Washington | 58S-22 | Used in the production of Hot Mix Asphalt (HMA) with less than 20 percent Reclaimed Asphalt Pavement (RAP) or without Recycled Asphalt Shingles (RAS). |
|  | 58H-22 | Suitable for HMA with moderate traffic levels or as specified in the contract. |
|  | 58V-22 | Used in HMA applications requiring higher binder performance for higher traffic levels. |
|  | 64S-28 | Used in colder climates requiring a binder that performs well at lower temperatures. |
|  | 64H-28 | Suitable for HMA with moderate to high traffic levels or as specified in the contract. |
|  | 64V-28 | Used in HMA applications requiring the highest binder performance for the highest traffic levels and low temperatures. |

## 3.3 South/Southeastern USA

In the South and Southeastern regions of the USA, states including Alabama, Florida, Georgia, and others use PG binders tailored to their hot and humid climates, as detailed in Table 3.2. These regions prioritize binders capable of withstanding high temperatures and preventing rutting. Standard binders such as PG 58-22 and PG 64-22 are widely used, while PG 76-22 PMA is favored in areas that require extra resilience. Additionally, states like Florida and Louisiana often utilize binders modified with ground tire rubber, such as PG 76-22 ARB, to enhance the pavement’s resistance to rutting and increase its flexibility.

Table 3.2. PG binders in the South/Southeastern USA

| State | PG Binders | Application & Comments |
| --- | --- | --- |
| Alabama | 58-22 | Table No. 1 in the Asphalt Materials section |
|  | 64-22 | Table No. 2 in the Asphalt Materials section |
|  | 67-22 | Table No. 3 in the Asphalt Materials section |
|  | 76-22 | Table No. 4 in the Asphalt Materials section |
| Arkansas | 64-22 | In moderate climates (SB, SBS, SBR are Modifiers for PG 70-22 and PG 76-22) |
|  | 70-22 | in warmer and hotter climates, respectively, often for highways and runways. (SB, SBS, SBR are Modifiers for PG 70-22 and PG 76-22) |
|  | 76-22 |  |
| Florida | 52-28 | Used in areas with lower temperature requirements. |
|  | 58-22 | Commonly used in general applications for moderate climates. |
|  | 67-22 | Suitable for higher temperature regions. |
|  | 76-22 PMA | Used in areas requiring higher temperature resistance and increased durability. (Produced with styrene-butadiene-styrene (SBS) or styrene-butadiene (SB)) |
|  | 76-22 ARB | Used in applications needing additional flexibility and resistance to rutting. (Contains a minimum of 7.0% ground tire rubber (GTR) by weight and may include polymer.) |
| Georgia | 52-XX | Used in a variety of paving applications based on regional climatic conditions and performance needs. |
|  | 58-XX |  |
|  | 64-XX |  |
|  | 64-28 TR+ | Designed for regions with extreme temperature variations, providing a balance between high-temperature stability and low-temperature flexibility. (Minimum of 8% crumb rubber and 2% SBS) |
|  | 70-22 TR+ | Suitable for use in asphalt mixtures where enhanced performance in terms of elasticity and resistance to deformation is required. (Minimum of 8% crumb rubber and 2% SBS) |
|  | 76-22 TR+ | Used for high-performance asphalt mixtures requiring superior resistance to rutting and thermal cracking. (Minimum of 8% crumb rubber and 2% SBS) |
| Kentucky | 58-22 | Used in asphalt materials to provide a workable plastic mixture. Heated separately to 300°F before combining. |
|  | 58-28 | Used in asphalt mixtures requiring a specific performance grade. |
|  | 64-22 | Used in asphalt mixtures and binders conforming to Section 806. (Used for leveling and wedging as per Subsection 403.05.) |
|  | 76-22 Modified | Used in asphalt mixtures requiring enhanced performance, especially in high-temperature environments. Must have a minimum Elastic Recovery (ER) at 10°C of 70 percent. |
| Louisiana | 58-28 | Required when 21-30% RAP is used in the mixture. |
|  | 67-22 | Used in Dense Mix, Coarse Mix, and OGFC (Open Graded Friction Course) as specified in Table 501-1. |
|  | 70-22 Modified | Used in Dense Mix, Coarse Mix, and OGFC; meets PG 70-22 requirements when latex additive is blended. |
|  | 76-22 Modified | Used in Dense Mix, Coarse Mix, and OGFC. |
|  | 82-22 Rubber Modified | Used when 30 mesh (or finer) crumb rubber is added to a PG 67-22 material. |
| Mississippi | 58-28 | Can be used in lieu of petroleum asphalt cement, Grade AC-10. |
|  | 67-22 | General bituminous material used in all types of asphalt mixtures. |
|  | 76-22 | Used in polymer modified asphalt mixtures and Open Graded Friction Course (OGFC) mixtures. |
|  | 82-22 | Used in polymer modified asphalt mixtures. |
| North Carolina | 64-22 | Asphalt binder for tack coat, asphalt concrete base, intermediate, and surface courses. |
|  | 70-22 | Asphalt concrete intermediate and surface courses. |
|  | 76-22 | Asphalt concrete intermediate and surface courses, ultra-thin bonded wearing course (UBWC). |
|  | 58-28 | Used with RAP or RAS in specific conditions. |
|  | 70-28 | Used in ultra-thin bonded wearing course (UBWC). |
|  | PMA | For plant mix. |
| Oklahoma | 58-28 (58S-28) | General use in asphalt cement. |
|  | 64-22 (64S-22) |  |
|  | 70-28 (64V-28) |  |
|  | 76-28 (64E-28) |  |
|  | 88-28 (76E-28) |  |
| South Carolina | 58-22 | Not explicitly detailed in the provided text but by using some materials like SBS they modify it for emulsion using. |
|  | 64-22 | Intermediate and Surface layers on Interstates; Primary and Secondary routes. |
|  | 76-22 | Intermediate and Surface layers on Interstates; Critical Areas; Used in Open-Graded Friction Course (OGFC) |
|  | 82-22 | Not explicitly detailed in the provided text. |
| Texas | 58-XX | Is used according to the requirements. |
|  | 64-XX |  |
|  | 70-XX |  |
|  | 76-XX |  |
|  | 82-XX |  |
|  | 64-22 | Hot-mixed, hot-laid asphalt mixtures, precoating, tack coat. |
|  | 76-22 | Dense-Graded Hot-Mix Asphalt, Superpave Mixtures, etc. |
|  | 70-22 | Substitute PG binder for original specifications. |
|  | 64-28 |  |
|  | 58-28 |  |
|  | 64-34 |  |
|  | 58-34 |  |
| Virginia | 64S-22 | Surface mixes (SM-4.75A, SM-9.0A, SM-9.5A, SM-12.5A), Intermediate mix (IM-19.0A), Base mix (BM-25.0A) |
|  | 64H-22 | Surface mixes (SM-4.75D, SM-9.0D, SM-9.5D, SM-12.5D), Intermediate mix (IM-19.0D), Base mix (BM-25.0D), SMA mixes (SMA-9.5, SMA-12.5, SMA-19.0) |
|  | 64E-22 | Type E asphalt mixtures, Surface mixes (SM-4.75E, SM-9.0E, SM-9.5E, SM-12.5E), Intermediate mix (IM-19.0E), SMA mixes (SMA-9.5, SMA-12.5, SMA-19.0) |
|  | 76E-22 | Polymer-modified asphalt, SMA mixes |
|  | 76E-28(HP) | High polymer binder mixes, Type E (HP) asphalt mixtures |
|  | 64H-16 | Used in BM-25.0D (+0.4 and +0.8) mixes. |
|  | 64S-22 | Used in BM-25.0D (+0.4 and +0.8) mixes with 25.0 ≤ %RAP ≤ 35.0. |
|  | 64H-22 | Used in BM-25.0D (+0.4 and +0.8) mixes with %RAP < 25.0. |

## 3.4 Midwest USA

The Midwest USA employs a variety of PG binders, carefully chosen to address the region's climate and traffic patterns, as shown in Table 3.3. Each state, including Illinois and Minnesota, specifies binders to ensure their pavements perform well under diverse conditions. The table details the range of PG binders used, from PG 64-22 to PG 70-28, with many incorporating modifications like SBS or SBR to combat thermal cracking and rutting. The Midwest's temperature extremes necessitate this tailored approach to binder selection.

Table 3.3. PG binders in the Midwest USA

| State | PG Binders | Application & Comments |
| --- | --- | --- |
| Illinois | 46-28 | General use in hot-mix asphalt (HMA) as specified in the plans. |
|  | 52-28 |  |
|  | 58-22 |  |
|  | 58-28 |  |
|  | 64-22 |  |
|  | 64-28 SB/SBS Modified | Enhanced performance characteristics for specific uses, particularly where higher resistance to rutting and cracking is required. |
|  | 70-22 SB/SBS Modified |  |
|  | 70-28 SB/SBS Modified |  |
|  | 76-22 SB/SBS Modified |  |
|  | 76-28 SB/SBS Modified |  |
|  | 64-28 SBR Modified |  |
|  | 70-22 SBR Modified |  |
|  | 70-28 SBR Modified |  |
|  | 76-22 SBR Modified |  |
|  | 76-28 SBR Modified |  |
| Indiana | 58-28 | These binders are used in various asphalt paving projects, depending on the specific requirements of the project, such as temperature and traffic conditions. |
|  | 64-22 |  |
|  | 64-28 |  |
|  | 70-22 |  |
|  | 70-28 |  |
|  | 76-22 |  |
|  | 58-28 Modified | Modified binders are used to improve the performance of asphalt in terms of elasticity and resistance to deformation, especially in high-stress areas. (Can be modified by styrene butadiene rubber (SBR)) |
|  | 64-22 Modified |  |
| Iowa | 58-28 | Used for various types of asphalt mixtures in road construction, ensuring durability and performance under different climatic conditions. |
|  | 64-22 |  |
|  | 64-34 |  |
|  | 70-28 |  |
|  | 58-34E+ | Used for flexible pavements, providing enhanced resistance to rutting and fatigue. |
|  | 64-34E+ |  |
| Kansas | 58-22 | Maintenance overlays |
|  | 64-22 | Maintenance overlays, can replace PG 58-22 |
|  | 70-28 Modified | Reflective Crack Interlayer (RCI) |
|  | 70-28 RCI Modified |  |
| Michigan | 46-34 | Various pavement design temperature requirements. |
|  | 46-40 |  |
|  | 46-46 |  |
|  | 52-10 |  |
|  | 52-16 |  |
|  | 52-22 |  |
|  | 52-28 |  |
|  | 52-34 |  |
|  | 52-40 |  |
|  | 52-46 |  |
|  | 58-16 |  |
|  | 58-22 |  |
|  | 58-28 |  |
|  | 58-34 |  |
|  | 58-40 |  |
|  | 64-10 |  |
|  | 64-16 |  |
|  | 64-22 |  |
|  | 64-28 |  |
|  | 64-34 |  |
|  | 64-40 |  |
|  | 70-10 |  |
|  | 70-16 |  |
|  | 70-22 |  |
|  | 70-28 |  |
|  | 70-34 |  |
|  | 70-40 |  |
|  | 76-10 | High-temperature performance requirements. |
|  | 76-16 |  |
|  | 76-22 |  |
|  | 76-28 |  |
|  | 76-34 |  |
|  | 82-10 |  |
|  | 82-16 |  |
|  | 82-22 |  |
|  | 82-28 |  |
|  | 82-34 |  |
|  | 64-28 PMA | Asphalt binder for general paving in specified regions. (North of M-72 in the Lower Peninsula and Upper Peninsula) |
|  | 70-22 PMA | Asphalt binder for general paving in specified regions. (South of M-72 (including M-72)) |
|  | 70-28 PMA | Asphalt binder for general paving in specified regions. (MDOT Metro Region only) |
| Minnesota | 58S-28 | General use |
|  | 58H-28 | Used in areas with heavy traffic loads |
|  | 58V-28 | Used in areas with very heavy traffic loads |
|  | 58E-28 | Used in areas with extremely heavy traffic loads |
|  | 58S-34 | Used in areas requiring better performance at low temperatures |
|  | 58H-34 | Used in areas with heavy traffic loads and requiring better performance at low temperatures |
|  | 58V-34 | Used in areas with very heavy traffic loads and requiring better performance at low temperatures. (Can be Polymer Modified Emulsion membrane for ultrathin bonded wearing course) |
|  | 58E-34 | Used in areas with extremely heavy traffic loads and requiring better performance at low temperatures |
|  | 49S-34 | Used in specific conditions as indicated by the grade. (Can be used in various recycled material mixtures.) |
|  | 52S-34 | Used in areas requiring specific performance at low temperatures. (Can be used in various recycled material mixtures.) |
|  | 64S-22 | Used in areas requiring better performance at higher temperatures. (Can be used in various recycled material mixtures.) |
| Missouri | 64-22 | General use in various asphalt mixtures including those with reclaimed asphalt pavement (RAP) and reclaimed asphalt shingles (RAS)​. |
|  | 52-28 | Used when the virgin binder ratio to total binder in the mixture is between 60% and 70%. |
|  | 58-28 |  |
|  | 46-28 | Spray application and general use in asphalt mixtures. The specific spraying temperature range for this binder is noted as 260-325°F. |
|  | 70-22 | General use in higher temperature applications, as specified in contracts. |
|  | 76-22 |  |
| Nebraska | 58S-34 | General asphalt concrete pavements. |
|  | 58H-34 | High traffic roads require improved resistance to deformation. |
|  | 58V-34 | Very high traffic roads and intersections. |
|  | 58E-34 | Extreme traffic conditions such as major urban roads and heavy truck routes. |
|  | XX-XX PMA | Used in applications requiring enhanced performance such as resistance to rutting and fatigue. They must meet the MSCR specifications and incorporate elastomer modifiers like SB, SBS, or SBR. |
| North Dakota | In their specifications, they did not directly mention any specific binders but instead used general requirements. |  |
| Ohio | 64-28 | Used in intermediate and base courses. |
|  | 64-22 | Used in intermediate courses and specific surface applications. |
|  | 58-28 | Used when a softer binder is required, such as in high RAP mixtures. |
|  | 64-22 SBR Modified | Used in fine graded polymer asphalt concrete (Type B). |
|  | 76-22 SBR Modified |  |
|  | 70-22M | Used in surface courses. |
|  | 76-22M | Used in surface courses and other applications requiring high-temperature performance. |
|  | 88-22M | Used in high-performance applications. |
| South Dakota | 58-34 | Used in various types of asphalt pavements to meet specific performance criteria. |
|  | 64-28 | Typically used for surface layers in moderate climate conditions to ensure durability and performance. |
|  | 64-34 | Used in surface layers for improved performance in colder climates. |
|  | 70-28 | Utilized for heavy traffic areas to provide better resistance to rutting and thermal cracking. |
|  | 70-34 | Employed in areas requiring higher performance in both high and low-temperature extremes. |
| Wisconsin | Do not change the PG binder grade without the engineer's written approval. The department will designate the grade of virgin asphaltic binder in the contract, however, the contractor may use virgin binder, modified binder, a blend of virgin and recovered binder, or a blend of modified and recovered binder. |  |

## 3.5 Western USA

In the Western USA, states such as Alaska, California, and Nevada select PG binders that meet the diverse climatic and traffic challenges of the region, with detailed specifications provided in Table 3.4. For instance, Alaska often utilizes PG 52-28 to cope with its cold climate, while hotter states like Arizona and California rely on modified binders such as PG 76-22 for areas with high temperatures and traffic volumes. Rubber-modified binders are also commonly used in states like Nevada and New Mexico to improve pavement performance under extreme conditions, while Utah and Washington focus on binders that balance temperature resilience and traffic load. Wyoming prefers binders like PG 76-XX to manage heavy traffic and high temperatures.

Table 3.4. PG binders in the Western USA

| State | PG Binders | Application & Comments |
| --- | --- | --- |
| Alaska | 52-28 | The entire document mentions the default PG grade if no other grade is specified. |
| Arizona | 52-34 | In moderate to hot climates (TR+ variants include crumb rubber and polymer modifications.) |
|  | 58-28 |  |
|  | 64-22 |  |
|  | 70-22 | in warmer and hotter climates, respectively, often for highways and runways. (TR+ variants include crumb rubber and polymer modifications.) |
|  | 76-16 |  |
|  | 76-22 |  |
| California | 58-22 | Used in various paving applications depending on the specific climate and traffic conditions they are designed to withstand. |
|  | 58-16 |  |
|  | 64-10 |  |
|  | 64-16 |  |
|  | 64-28 |  |
|  | 70-10 |  |
|  | 58-34 Modified | Suitable for cooler climates where low-temperature cracking is a concern. |
|  | 64-28 Modified | Used in moderate climates with moderate traffic load and weather conditions. |
|  | 76-22 Modified | Ideal for high-traffic areas and regions with extreme temperature variations, providing resistance to rutting and fatigue cracking. |
| Colorado | 58-28 | Used in Superpave asphalt mixtures for road construction and maintenance. |
|  | 58-34 |  |
|  | 64-22 |  |
|  | 64-28 |  |
|  | 70-28 |  |
|  | 76-28 |  |
| Hawaii | 64-16 | Used for tack coat in thin lift maintenance contracts, typically less than 1 1/4 inches thick. |
| Idaho | 58-28 | General use in asphalt mixtures. |
|  | 58-34 | Adjusted binder grade for higher low-temperature performance. |
|  | 64-28 | Used in Superpave HMA mixtures, general use. |
|  | 64-34 | Adjusted binder grade for higher low-temperature performance. |
|  | 70-28 | Used in Superpave HMA mixtures, heavy traffic areas. |
|  | 70-34 | Adjusted binder grade for higher low-temperature performance. |
|  | 76-28 | Used in Superpave HMA mixtures, high-stress areas. |
|  | 58-28 Modified | Requires at least 50 percent elastic recovery, used in specific high-performance applications. |
|  | 58-34 Modified | Adjusted binder grade for higher low-temperature performance with polymer modification. |
| Montana | 64-28 | General paving use after aging in the rolling thin film oven and testing in accordance with AASHTO T 51. |
|  | 64-34 |  |
|  | 70-28 |  |
|  | 58-28 | Meets the dynamic shear requirements for original and RTFO residue for specific temperature grades. |
|  | 64-22 |  |
| Nevada | 58-28 | General use in pavement constructions where moderate climates are expected. |
|  | 64-16 | Used in pavements subjected to moderate temperature variations. |
|  | 64-22 | Suitable for pavements in areas with higher temperature fluctuations. |
|  | 70-16 | Typically used in high-temperature regions to prevent rutting. |
|  | 64-28NV | Used in specific Nevada applications requiring additional performance criteria. |
|  | 76-22NV | Modified binder used for enhanced performance in extreme temperature conditions. |
|  | 64-28NVTR | Rubber-modified binder for enhanced elasticity and durability in extreme conditions. |
|  | 76-22NVTR | Rubber-modified binder used in regions with severe climate to improve performance. |
| New Mexico | 64-22 | Standard paving applications |
|  | 58-28 | Used in colder climates where lower temperatures are a concern |
|  | 76-22+ Modified | High-performance applications requiring enhanced durability and resistance to rutting |
|  | 76-28+ Modified | High-performance applications requiring resistance to both rutting and low-temperature cracking |
|  | 70-22+ Modified | Applications requiring improved performance over standard grades |
|  | 70-28+ Modified | Applications requiring resistance to both rutting and low-temperature cracking |
|  | 76-28R+ Modified | Applications incorporating recycled materials, needing high resistance to rutting and cracking |
|  | 70-28R+ Modified | Applications incorporating recycled materials, needing balanced performance in various conditions |
| Oregon | 64-22 | These binders can be substituted for the specified grade of asphalt cement for guardrail flares, mailbox turnouts, road approaches, driveways, and non-travel lane areas of restricted widths that are less than 8 ft. |
|  | 64-28 |  |
| Utah | 58-34 | General use in hot mix asphalt (HMA) pavements for low and intermediate traffic volumes and temperatures. |
|  | 64-28 | Suitable for moderate climate conditions and used in a variety of HMA pavements for intermediate traffic volumes. |
|  | 64-34 | Designed for colder temperatures, used in HMA pavements requiring greater resistance to thermal cracking. |
|  | 70-22 | Used in HMA pavements designed for high temperatures and heavy traffic conditions. |
|  | 70-28 | Designed for areas with high temperatures and moderate traffic volumes. |
|  | 70-34 | Used in HMA pavements requiring resistance to both high temperatures and low-temperature cracking. |
|  | 76-22 | Suitable for extremely high temperatures and heavy traffic loads. |
|  | 76-28 | Used in HMA pavements exposed to extreme temperature ranges and heavy traffic volumes. |
| Washington | 58S-22 | Used in the production of Hot Mix Asphalt (HMA) with less than 20 percent Reclaimed Asphalt Pavement (RAP) or without Recycled Asphalt Shingles (RAS). |
|  | 58H-22 | Suitable for HMA with moderate traffic levels or as specified in the contract. |
|  | 58V-22 | Used in HMA applications requiring higher binder performance for higher traffic levels. |
|  | 64S-28 | Used in colder climates requiring a binder that performs well at lower temperatures. |
|  | 64H-28 | Suitable for HMA with moderate to high traffic levels or as specified in the contract. |
|  | 64V-28 | Used in HMA applications requiring the highest binder performance for the highest traffic levels and low temperatures. |
| Wyoming | 58-XX | Suitable for areas with moderate temperature fluctuations. Often used in base or intermediate layers of pavements. |
|  | 64-XX | Commonly used in regions with a higher range of temperatures. Typically used for surface layers due to its balance of stiffness and flexibility. |
|  | 70-XX | Used in areas with high temperature ranges. Suitable for high-stress areas such as intersections and heavy traffic roads. |
|  | 76-XX | Ideal for extremely high-temperature regions or areas with heavy traffic loads. Provides excellent rutting resistance. |

# LTPP Database

## 4.1 Introduction

The LTPP database serves as a vast and invaluable repository of pavement performance data gathered from a wide range of test sections across North America. Since its inception, the LTPP database has accumulated an extensive collection of information on pavement materials, structures, and their performance under diverse environmental and traffic conditions. This section of the report focuses specifically on the analysis of modified and highly modified binders within the LTPP database. The objective is to identify pavement sections where these advanced materials have been implemented. Understanding how modified binders perform in real-world conditions is crucial for advancing pavement technology and ensuring longer-lasting, more resilient roadways.

However, modified binders should be viewed as a representative of a broader category of innovative paving materials. These materials, such as RAP, RAS, and warm-mix asphalt, have been increasingly adopted in modern pavement construction. Their use aims to improve pavement durability, reduce environmental impacts, and extend service life—objectives that align with those of modified binders. Therefore, while the current analysis focuses on modified binders, it sets the stage for future studies to explore the potential of other innovative materials in enhancing pavement performance.

To accurately determine the types of binders used in various pavement sections, two primary methods are employed: the Standard Data Release (SDR) and the Analysis-Ready Materials Dataset (ARMAD). Each method offers distinct advantages for extracting and analyzing the relevant data.

The SDR is an exhaustive resource that provides detailed records of materials used in various pavement sections across North America. This file contains comprehensive data on the types of asphalt binders, their physical and chemical properties, and their specific application areas within the pavement structure. The SDR is instrumental for tracking the evolution of materials used in different roadway projects over time. It offers a historical perspective on how various binders have been selected, modified, and applied in response to changing project demands, environmental factors, and technological advancements. By leveraging the SDR, researchers and engineers can trace the use of specific binders in past and present pavement sections, thereby gaining insights into their long-term performance.

On the other hand, the ARMAD provides a streamlined and ready-to-analyze collection of data on materials used in pavement sections, with a particular focus on asphalt binders. ARMAD is designed to facilitate more efficient and detailed analysis by offering pre-processed data that is immediately accessible for performance evaluation. This dataset includes critical information on binder types, formulations, and modifications, allowing for a more in-depth examination of how different binders perform under various environmental and traffic conditions. ARMAD’s ready-to-use data structure is particularly advantageous for conducting comparative studies, identifying trends, and developing predictive models related to binder performance.

Utilizing both the SDR and ARMAD methods enables a comprehensive approach to data gathering and analysis. The SDR provides a broad, historical view of binder usage, while ARMAD offers the tools necessary for detailed, performance-focused investigations. Together, these resources empower researchers and engineers to effectively assess the suitability and longevity of different asphalt binders, particularly modified binders, in real-world applications. This dual-method approach supports informed decision-making in the selection of materials that can enhance pavement performance, durability, and overall lifecycle cost-effectiveness.

As the use of modified binders has paved the way for better pavement performance, expanding the research to include other innovative materials such as RAP and RAS will allow transportation agencies to explore their potential benefits more comprehensively. These materials, much like modified binders, hold significant promise for advancing pavement sustainability, reducing lifecycle costs, and improving the overall durability of transportation infrastructure. By incorporating them into future research frameworks and databases, we can ensure a more comprehensive understanding of innovative material applications in pavement engineering.

## 4.2 Standard Data Release (SDR)

In the SDR method, the Material Test File and Inventory File are two resources for obtaining information about different binders in various sections of the LTPP database. The Material Test File provides detailed results from tests conducted on asphalt binders, offering insights into their properties and composition, which are crucial for evaluating binder performance. Meanwhile, the Inventory File offers a comprehensive summary of the materials used in each pavement section, including the type and grade of binders, allowing for easy identification of binder usage across different sections. Together, these files enable researchers and engineers to extract and analyze critical data on binders, supporting a deeper understanding of material performance in the LTPP database.

### 4.2.1 Material Test File

The material test file includes various experiments identified by specific codes, each detailed in Table 4.1, which helps in detecting relevant projects. For this project, which aims to investigate modified and highly modified binders within the LTPP database, particular attention should be focused on two specific codes: 6C and 7C. Code 6C corresponds to “AC Overlay with Modified Asphalt Cement on AC Pavement, No Milling”, while code 7C refers to “AC Overlay with Modified Asphalt Cement on PCC Pavement, with CPR or No Pretreatment”. These codes are necessary for the investigation, as they directly relate to projects involving modified asphalt cement overlays, which are essential for studying modified binders.

Table 4.1. Experiment codes and descriptions for LTPP projects (FHWA-RD-05-083, July 2005)

| CODE | DETAIL |
| --- | --- |
| 1 | Asphalt Concrete on Unbound Granular Base |
| 2 | Asphalt Concrete on Bound Base |
| 3 | Jointed Plain Concrete Pavement (JPCP) |
| 4 | Jointed Reinforced Concrete Pavement (JPCP) |
| 5 | Continuously Reinforced Concrete Pavement (CRCP) |
| 6A | Existing AC Overlay on AC Pavement |
| 6B | AC Overlay with Conventional Asphalt Cement on AC Pavement, No Milling |
| 6C | AC Overlay with Modified Asphalt Cement on AC Pavement, No Milling |
| 6D | Multiple AC Overlays with Conventional Asphalt Cement on AC Pavement, No Milling |
| 6S | AC Overlay on AC Pavement with Milling and/or Fabric Pretreatment |
| 7A | Existing AC Overlay on PCC Pavement |
| 7B | AC Overlay with Conventional Asphalt Cement on PCC Pavement, with CPR or No Pretreatment |
| 7C | AC Overlay with Modified Asphalt Cement on PCC Pavement, with CPR or No Pretreatment |
| 7D | Multiple AC Overlays with Conventional Asphalt Cement on PCC Pavement, with No Pretreatment |
| 7F | AC Overlay on PCC Pavement, with Slab Fracture Pretreatment |
| 7R | Intensive Concrete Pavement Restoration of PCC without Overlay |
| 7S | AC Overlay on PCC Pavement with Pretreatment |
| 9 | Unbonded PCC Overlay of PCC Pavement |
| 1 | Strategic Study of Structural Factors for Flexible Pavements, new/reconstructed AC pavements |
| 2 | Strategic Study of Structural Factors for Rigid Pavements, new/reconstructed JPCC pavements |
| 3 | Preventive Maintenance of AC Pavement |
| 4 | Preventive Maintenance of Jointed Concrete Pavement |
| 5 | AC Overlay of AC Pavement |
| 6 | Rehabilitation of Jointed PCC Pavement |
| 7 | Bonded Concrete Overlay on Portland Cement Concrete Pavement |
| 8 | Study of Environmental Effects in the Absence of Heavy Loads |
| 9A | Superpave Asphalt Binder Study (Project Level Designation) |
| 9C | Superpave Asphalt Binder Study, AC Overlay on CRCP) |
| 9J | Superpave Asphalt Binder Study, AC Overlay on JCP) |
| 9N | Superpave Asphalt Binder Study, New AC Pavement Construction) |
| 9O | Superpave Asphalt Binder Study, AC Overlay on AC Pavement) |
| 9P | Pilot Superpave Asphalt Binder Study (Project Level Designation) |
| 10 | Warm Mix Asphalt Overlay of Asphalt Pavement |

After conducting data mining, all sections classified under “AC Overlay with Modified Asphalt Cement on AC Pavement, No Milling” and “AC Overlay with Modified Asphalt Cement on PCC Pavement, with CPR or No Pretreatment” have been compiled and are presented in Tables 4.2 and 4.3. In the 6C category, the sections are distributed as follows: Arizona (1), California (15), Colorado (5), Delaware (4), Florida (1), Georgia (1), Idaho (2), Maryland (1), Mississippi (2), North Carolina (9), Ohio (2), Oklahoma (1), Pennsylvania (1), South Dakota (3), Texas (2), Virginia (16), Washington (2), Wyoming (3), and Quebec (6). For the 7C category, the sections are distributed as follows: Alabama (1), California (1), Delaware (1), Illinois (1), Iowa (17), Kansas (1), Nebraska (1), North Carolina (1), Ohio (6), Oregon (2), Pennsylvania (6), Texas (5), and Quebec (1). The numbers in brackets indicate the section numbers from the available data in the LTPP database. These tables demonstrate the widespread use of modified pavement or overlay across 24 states in the United States and Canada, reflecting its application in diverse climatic and geographical conditions.

Table 4.2. Sections classified under “AC Overlay with Modified Asphalt Cement on AC Pavement, No Milling”

| STATE | STATE CODE | SHRP ID | CONSTRUCTION NO | GPS/SPS | EXPERIMENT NO |
| --- | --- | --- | --- | --- | --- |
| Arizona | 4 | 6055 | 3 | G | 6C |
| California | 6 | 7452 | 3 | G | 6C |
|  |  | 7454 | 2 | G | 6C |
|  |  | 2002 | 6 | G | 6C |
|  |  | 8534 | 5 | G | 6C |
|  |  | 8535 | 5 | G | 6C |
|  |  | 8534 | 6 | G | 6C |
|  |  | 8534 | 4 | G | 6C |
|  |  | 2038 | 5 | G | 6C |
|  |  | 8535 | 4 | G | 6C |
|  |  | 8149 | 5 | G | 6C |
|  |  | 7491 | 4 | G | 6C |
|  |  | 8156 | 8 | G | 6C |
|  |  | 2002 | 7 | G | 6C |
|  |  | 8535 | 6 | G | 6C |
| Colorado | 8 | 6002 | 3 | G | 6C |
|  |  | 7781 | 5 | G | 6C |
|  |  | 7781 | 6 | G | 6C |
|  |  | 6002 | 2 | G | 6C |
|  |  | 1053 | 2 | G | 6C |
| Delaware | 10 | 1450 | 4 | G | 6C |
|  |  | 1450 | 5 | G | 6C |
|  |  | 1450 | 6 | G | 6C |
|  |  | 1450 | 3 | G | 6C |
| Florida | 12 | 4096 | 2 | G | 6C |
| Georgia | 13 | 4096 | 2 | G | 6C |
| Idaho | 16 | 1020 | 5 | G | 6C |
|  |  | 1020 | 4 | G | 6C |
| Maryland | 24 | 1634 | 2 | G | 6C |
| Mississippi | 28 | 3087 | 3 | G | 6C |
|  |  | 3087 | 2 | G | 6C |
| North Carolina |  | 1992 | 2 | G | 6C |
|  |  | 1352 | 4 | G | 6C |
|  |  | 2824 | 2 | G | 6C |
|  |  | 2819 | 2 | G | 6C |
|  |  | 1817 | 5 | G | 6C |
|  |  | 1817 | 6 | G | 6C |
|  |  | 1352 | 3 | G | 6C |
|  |  | 1817 | 4 | G | 6C |
|  |  | 2819 | 3 | G | 6C |
| Ohio | 39 | 0111 | 3 | G | 6C |
|  |  | 0111 | 2 | G | 6C |
| Oklahoma | 40 | 4087 | 2 | G | 6C |
| Pennsylvania | 42 | 1599 | 3 | G | 6C |
| South Dakota | 46 | 0859 | 5 | G | 6C |
|  |  | 0804 | 2 | G | 6C |
|  |  | 0803 | 2 | G | 6C |
| Texas | 48 | 3865 | 2 | G | 6C |
|  |  | 3865 | 3 | G | 6C |
| Virginia | 51 | 2004 | 3 | G | 6C |
|  |  | 2004 | 2 | G | 6C |
|  |  | 1417 | 5 | G | 6C |
|  |  | 0118 | 3 | G | 6C |
|  |  | 0124 | 3 | G | 6C |
|  |  | 0116 | 3 | G | 6C |
|  |  | 0159 | 3 | G | 6C |
|  |  | 0123 | 3 | G | 6C |
|  |  | 0122 | 3 | G | 6C |
|  |  | 0121 | 3 | G | 6C |
|  |  | 0119 | 3 | G | 6C |
|  |  | 0117 | 3 | G | 6C |
|  |  | 0115 | 3 | G | 6C |
|  |  | 0114 | 3 | G | 6C |
|  |  | 0120 | 3 | G | 6C |
| Washington | 53 | 6048 | 2 | G | 6C |
|  |  | 6048 | 3 | G | 6C |
| Wyoming | 56 | 2017 | 5 | G | 6C |
|  |  | 2017 | 7 | G | 6C |
|  |  | 2017 | 6 | G | 6C |
| Quebec | 89 | 0901 | 2 | G | 6C |
|  |  | A903 | 2 | G | 6C |
|  |  | A902 | 2 | G | 6C |
|  |  | A901 | 2 | G | 6C |
|  |  | 0903 | 2 | G | 6C |
|  |  | 0902 | 2 | G | 6C |

Table 4.3. Sections classified under “AC Overlay with Modified Asphalt Cement on PCC Pavement, with CPR or No Pretreatment”

| State | STATE_CODE | SHRP_ID | CONSTRUCTION_NO | GPS_SPS | EXPERIMENT_NO |
| --- | --- | --- | --- | --- | --- |
| Alabama | 1 | 3998 | 3 | G | 7C |
| California | 6 | 7455 | 3 | G | 7C |
| Delaware | 10 | 5005 | 4 | G | 7C |
| Illinois | 17 | 5843 | 7 | G | 7C |
| Iowa | 19 | 0602 | 12 | G | 7C |
|  |  | 0605 | 11 | G | 7C |
|  |  | 0601 | 8 | G | 7C |
|  |  | 0601 | 7 | G | 7C |
|  |  | 0602 | 10 | G | 7C |
|  |  | 0601 | 10 | G | 7C |
|  |  | 0601 | 9 | G | 7C |
|  |  | 0602 | 9 | G | 7C |
|  |  | 0602 | 11 | G | 7C |
|  |  | 0605 | 12 | G | 7C |
|  |  | 0605 | 13 | G | 7C |
|  |  | 0605 | 14 | G | 7C |
|  |  | 0601 | 12 | G | 7C |
|  |  | 0602 | 13 | G | 7C |
|  |  | 0601 | 11 | G | 7C |
| Kansas | 20 | 3013 | 7 | G | 7C |
| Nebraska | 31 | 4019 | 7 | G | 7C |
| North Carolina | 37 | 3008 | 5 | G | 7C |
| Ohio | 39 | 4018 | 3 | G | 7C |
|  |  | 9006 | 5 | G | 7C |
|  |  | 3801 | 4 | G | 7C |
|  |  | 9006 | 4 | G | 7C |
|  |  | 3801 | 3 | G | 7C |
|  |  | 5003 | 4 | G | 7C |
| Oregon | 41 | 5006 | 2 | G | 7C |
|  |  | 5008 | 2 | G | 7C |
| Pennsylvania | 42 | 1606 | 4 | G | 7C |
|  |  | 1614 | 5 | G | 7C |
|  |  | 1623 | 3 | G | 7C |
|  |  | 1614 | 6 | G | 7C |
|  |  | 1623 | 4 | G | 7C |
| Texas | 48 | 5154 | 5 | G | 7C |
|  |  | 5335 | 3 | G | 7C |
|  |  | 5154 | 6 | G | 7C |
|  |  | 5154 | 4 | G | 7C |
|  |  | 5274 | 3 | G | 7C |
| Quebec | 89 | 3015 | 10 | G | 7C |

### 4.2.2 Inventory File

The Inventory File contains detailed records of asphalt binders used across various pavement sections, organized within a comprehensive database that includes multiple tables. The “INV_PMA_ASPHALT” table provides extensive information such as section identification numbers, state codes, construction numbers, layer numbers, asphalt binder grades, additional binder grade details, and sources of the binders. This content of this table is further illustrated in Table 4.4, which includes various parameters like Asphalt Grade (100%), Source (87.55%), Asphalt Specific Gravity (76.01%), Original Asphalt Viscosity at 140°F (66.30%) and 275°F (56.59%), Original Penetration at 77°F (68.86%), Original Ductility at 77°F (12.45%) and 39°F (0.55%), Lab Viscosity at 140°F (35.71%) and 275°F (9.34%), Lab Ductility at 77°F (25.46%) and 39°F (0.55%), and Lab Penetration at 77°F (18.32%) and 39°F (0.73%). The percentages represent the availability of the data from the possible data entries.

Additionally, the “INV_MODIFIER” table contains information about the types of modifiers used in different sections, with the asphalt cement modifier codes presented in Table 4.5. From the “INV_PMA_ASPHALT” table, different grades of asphalt can be extracted, each associated with a specific code representing a particular asphalt binder, as detailed in Table 4.6. This combined information is defined for tracking and analyzing the performance and characteristics of different binders used in construction and maintenance, making it a valuable resource for researchers and engineers.

Following an extensive data mining process, it was determined that only the sections listed in Table 4.7 of the report involved the use of modifiers within the LTPP database. This table specifically highlights those pavement sections where modified binders were employed, providing a focused subset of data for further analysis. The identification of these sections is crucial as it allows researchers to concentrate their efforts on evaluating the performance and effectiveness of modified asphalt binders, enabling a more targeted investigation into their impact on pavement durability and longevity under various conditions. By isolating these sections, the study can yield more precise insights into the benefits and challenges associated with the use of modifiers in asphalt pavements, contributing to the broader understanding of how these materials influence pavement performance over time.

Table 4.4. Content of “INV_PMA_ASPHALT” table

| Information | Percent |
| --- | --- |
| ASPHALT_GRADE | 100 |
| ASPHALT_GRADE_OTHER | 1.83 |
| SOURCE | 87.55 |
| SOURCE_OTHER | 37.73 |
| ASPHALT_SPECIFIC_GRAVITY | 76.01 |
| ORIG_ASPHALT_VISCOSITY_140 | 66.30 |
| ORIG_ASPHALT_VISCOSITY_275 | 56.59 |
| ORIG_PENETRATION_77 | 68.86 |
| ORIG_DUCTILITY_77 | 12.45 |
| ORIG_DUCTILITY_39 | 0.55 |
| ORIG_DUCTILITY_TEST_RATE | 0.00 |
| ORIG_PENETRATION_39 | 2.93 |
| ORIG_RING_BALL_SOFTENING_PT | 1.47 |
| LAB_AGE_TEST_PROC | 48.72 |
| LAB_AGE_TEST_PROC_OTHER | 4.03 |
| LAB_VISCOSITY_140 | 35.71 |
| LAB_VISCOSITY_275 | 9.34 |
| LAB_DUCTILITY_77 | 25.46 |
| LAB_DUCTILITY_39 | 0.55 |
| LAB_DUCTILITY_TEST_RATE | 0.18 |
| LAB_PENETRATION_77 | 18.32 |
| LAB_PENETRATION_39 | 0.73 |
| LAB_RING_BALL_SOFTENING_PT | 0.37 |
| LAB_WEIGHT_LOSS | 10.62 |
| RECORD_STATUS | 100.00 |
| Average | 27.76 |

Table 4.5. Different modifier in LTPP database (FHWA-RD-05-083, July 2005)

| Material | Code |
| --- | --- |
| Stone Dust | 01 |
| Lime | 02 |
| Portland Cement | 03 |
| Carbon Black | 04 |
| Sulfur | 05 |
| Lignin | 06 |
| Natural Latex | 07 |
| Synthetic Latex | 08 |
| Block Copolymer | 09 |
| Reclaimed Rubber | 10 |
| Polyethylene | 11 |
| Polypropylene | 12 |
| Ethylene-Vinyl Acetate | 13 |
| Polyvinyl Chloride | 14 |
| Asbestos | 15 |
| Rock Wool | 16 |
| Polyester | 17 |
| Manganese | 18 |
| Other Mineral Salts | 19 |
| Lead Compounds | 20 |
| Carbon | 21 |
| Calcium Salts | 22 |
| Recycling Agents | 23 |
| Rejuvenating Oils | 24 |
| Amines | 25 |
| Fly Ash | 26 |
| Other | 27 |

Table 4.6. Asphalt grade codes in LTPP database (FHWA-RD-05-083, July 2005)

| Asphalt Cements | Code |
| --- | --- |
| AC-2.5 | 01 |
| AC-5 | 02 |
| AC-10 | 03 |
| AC-20 | 04 |
| AC-30 | 05 |
| AC-40 | 06 |
| AR-1000 (AR-10 by AASHTO Designation) | 07 |
| AR-2000 (AR-20 by AASHTO Designation) | 08 |
| AR-4000 (AR-40 by AASHTO Designation) | 09 |
| AR-8000 (AR-80 by AASHTO Designation) | 10 |
| AR-16000 (AR-160 by AASHTO Designation) | 11 |
| 200-300 pen | 12 |
| 120-150 pen | 13 |
| 58-100 pen | 14 |
| 60-70 pen | 15 |
| 40-50 pen | 16 |
| Other Asphalt Cement Grade | 17 |

Table 4.7. Pavement sections utilizing modified binders identified in the LTPP database

| SHRP_ID | STATE | CONSTRUCTION_NO | LAYER_NO | ASPHALT_MODIFIER_TYPE |
| --- | --- | --- | --- | --- |
| 6002 | Colorado | 1 | 4 | 2 |
| 1004 | Georgia | 1 | 5 | 2 |
| 1004 | Georgia | 1 | 3 | 2 |
| 1004 | Georgia | 1 | 4 | 2 |
| 7075 | Montana | 1 | 4 | 2 |
| 7076 | Montana | 1 | 4 | 2 |
| 7075 | Montana | 1 | 5 | 2 |
| 1060 | Texas | 1 | 6 | 2 |
| 1004 | Utah | 1 | 3 | 2 |
| 1017 | Utah | 1 | 3 | 2 |
| 1007 | Utah | 1 | 6 | 2 |
| 1007 | Utah | 1 | 4 | 2 |
| 1006 | Utah | 1 | 5 | 2 |
| 1006 | Utah | 1 | 3 | 2 |
| 2037 | Wyoming | 1 | 3 | 2 |
| 6060 | Arizona | 1 | 5 | 3 |
| 1036 | Arizona | 1 | 3 | 3 |
| 3104 | Tennessee | 1 | 3 | 5 |
| 1028 | Tennessee | 1 | 3 | 5 |
| 1028 | Tennessee | 1 | 4 | 5 |
| 1028 | Tennessee | 1 | 5 | 5 |
| 1004 | Utah | 1 | 3 | 7 |
| 1006 | Utah | 1 | 3 | 8 |
| 1020 | Idaho | 1 | 4 | 25 |
| 2017 | Wyoming | 1 | 3 | 25 |
| 1001 | New Hampshire | 1 | 6 | 27 |
| 1030 | North Carolina | 1 | 4 | 27 |
| 1817 | North Carolina | 1 | 4 | 27 |
| 2819 | North Carolina | 1 | 4 | 27 |
| 2825 | North Carolina | 1 | 4 | 27 |
| 3011 | North Carolina | 1 | 2 | 27 |
| 1645 | North Carolina | 1 | 5 | 27 |
| 1802 | North Carolina | 1 | 4 | 27 |
| 1006 | North Carolina | 1 | 5 | 27 |
| 1992 | North Carolina | 1 | 4 | 27 |
| 1028 | North Carolina | 1 | 4 | 27 |
| 1024 | North Carolina | 1 | 4 | 27 |
| 2824 | North Carolina | 1 | 4 | 27 |
| 1049 | Texas | 1 | 6 | 27 |
| 1049 | Texas | 1 | 5 | 27 |
| 1007 | Wyoming | 1 | 3 | 27 |

## 4.3. Analysis-Ready Materials Dataset (ARMAD)

Table 4.8 provides a comprehensive list of the specific tables that have been created within the ARMAD database. Collectively, these tables encompass over one million records, illustrating the extensive nature of the data collection. Additionally, the number of records in the ARMAD tables is expected to grow significantly with the future integration of the SPS-10 laboratory testing data into subsequent SDRs. This planned incorporation will enhance the database's depth and utility, offering even more detailed insights for researchers and engineers.

Table 4.8. Content of analysis-ready materials dataset (ARMAD)

| No. | Table Name | Description |
| --- | --- | --- |
| 1 | ANALYSIS_TST_UNBOUND | Representative properties of unbound base, subbase, and subgrade materials. |
| 2 | ANALYSIS_TST_UNBOUND_SUPPORT | Support information for the unbound base, subbase, and subgrade material properties. |
| 3 | ANALYSIS_TST_PCC | Representative properties of PCC materials. |
| 4 | ANALYSIS_TST_PCC_SUPPORT | Support information for the PCC material properties. |
| 5 | ANALYSIS_TST_AC | Representative properties of AC materials. |
| 6 | ANALYSIS_TST_AC_SUPPORT | Support information for the AC material properties. |
| 7 | ANALYSIS_TST_AC_ESTAR | AC dynamic modulus data generated from an analysis study (Kim et al. 2011). No support table presently exists. |
| 8 | ANALYSIS_TST_AC_CREEP_COMP | AC creep compliance testing properties. |
| 9 | ANALYSIS_TST_AC_CRCOM_SUPPORT | Support information for the AC creep compliance values. |
| 10 | ANALYSIS_TST_ACT | Representative properties of ATB base and subbase testing materials. |
| 11 | ANALYSIS_TST_ACT_SUPPORT | Support information for the ATB base and subbase material properties. |
| 12 | ANALYSIS_TST_PCT | Representative properties of CTB base and subbase materials. |
| 13 | ANALYSIS_TST_PCT_SUPPORT | Support information for CTB base and subbase materials. |
| 14 | ANALYSIS_TST_TR | Representative properties of treatment layers. |
| 15 | ANALYSIS_TST_TR_SUPPORT | Support information for treatment layer types. |
| 16 | ANALYSIS_TST_EF | Representative properties of EF layers. |
| 17 | ANALYSIS_TST_EF_SUPPORT | Support table for EF layers. |

Among all the tables in the database, the “ANALYSIS_TST_AC” table represents a comprehensive collection of analytical data related to asphalt cements. This table includes various parameters such as material codes, descriptions, complex modulus values, phase angles, viscosities, penetration rates, air voids, aggregate properties, and other critical characteristics essential for detailed analysis of asphalt performance. The percentage values indicate the availability of each data parameter from the possible entries. Table 4.9 illustrates these detailed parameters, highlighting the breadth and depth of the data collected.

Table 4.9. Analysis of asphalt cement in ARMAD

| Information | Percent |
| --- | --- |
| MATL_CODE | 100.00 |
| DESCRIPTION | 100.00 |
| ESTAR_LINK_GROUP | 25.84 |
| DSR_COMPLEX_MODULUS_TANK | 0.23 |
| DSR_COMPLEX_PHASE_ANGLE_TANK | 0.03 |
| DSR_COMPLEX_MODULUS_RTFO | 0.18 |
| DSR_COMPLEX_PHASE_ANGLE_RTFO | 0.03 |
| DSR_COMPLEX_MODULUS_PAV | 0.18 |
| DSR_COMPLEX_PHASE_ANGLE_PAV | 0.03 |
| IDT_AVERAGE | 10.95 |
| IDT_TEST_TEMPERATURE | 10.95 |
| IDT_LOADING_RATE | 78.48 |
| ABSOLUTE_VISC_140_F | 13.31 |
| KINEMATIC_VISC_275_F | 13.33 |
| IDT_POISSON_USED | 14.95 |
| POISSON_RATIO_TEST_TEMP | 78.48 |
| AIR_VOIDS_AVG_WP | 4.07 |
| AIR_VOIDS_AVG_NWP | 6.27 |
| ONE_AND_HALF_PASSING | 14.70 |
| ONE_PASSING | 14.65 |
| THREE_FOURTHS_PASSING | 14.66 |
| ONE_HALF_PASSING | 14.54 |
| THREE_EIGHTHS_PASSING | 14.54 |
| NO_4_PASSING | 14.65 |
| NO_10_PASSING | 14.58 |
| NO_40_PASSING | 14.58 |
| NO_80_PASSING | 14.58 |
| NO_200_PASSING | 14.65 |
| ASPHALT_CONTENT_MEAN | 13.75 |
| MAX_SPEC_GRAVITY | 14.96 |
| BSG | 4.92 |
| THERMAL_CONDUCTIVITY | 78.48 |
| HEAT_CAPACITY | 78.48 |
| SUR_SHORTWAVE_ABSORP | 78.48 |
| COEF_THERMAL_CONTRACTION | 78.48 |
| AGGR_SPEC_GRAVITY | 78.48 |
| BINDER_SPEC_GRAVITY | 78.48 |
| VOIDS_MINERAL_AGGR | 3.12 |
| VOIDS_FILLED_ASPHALT | 3.08 |
| CREEP_COMP_LINK | 6.54 |
| PROJECT_LAYER_CODE | 64.85 |
| Average | 28.92 |

# Discussions

## 5.1 Overview

This section starts by providing a comprehensive summary and analysis of the specifications from various DOTs, with a particular focus on the types of asphalt binder modifications adopted across different states. The discussion explores the rationale behind these modifications, the materials and technologies used, and the specific conditions under which they are applied. By understanding the variation in DOT practices, we can gain insight into regional preferences and the effectiveness of different modification strategies in addressing local pavement challenges.

Following the review of DOT specifications, the focus shifts to the data available within the LTPP database. This portion of the report critically examines the advantages and disadvantages of the database, identifying key areas where the data is robust as well as where it falls short. One of the major concerns highlighted is the noticeable gap in the LTPP database regarding detailed information on modified and highly modified binders. This lack of data poses significant challenges for researchers and engineers attempting to evaluate the long-term performance and benefits of these materials. The discussion will delve into the implications of these data gaps, considering how they limit the ability to conduct comprehensive analyses and draw reliable conclusions about the effectiveness of modified binders.

Moreover, this section will discuss the impact of the missing data on the broader pavement research community, including how it hampers efforts to develop predictive models and make informed decisions about pavement design and maintenance. By addressing these shortcomings, the report aims to emphasize the need for more comprehensive data collection and suggest areas for future improvement in both the LTPP database and other related datasets. This expanded discussion underscores the critical importance of accurate and complete data in advancing the understanding and application of modified and highly modified binders in pavement engineering.

## 5.2 Comparison of DOT Specifications for Asphalt Binder Modifications

The selection of asphalt binders and their modification has become a pivotal element in pavement design to address regional climatic challenges, traffic demands, and specific performance requirements of modern infrastructure. The U.S. Department of Transportation across various states has established tailored specifications for asphalt binder modifications, reflecting the diverse environmental conditions and operational needs. According to Chapter 3 data, these specifications vary significantly across different U.S. regions, including the Northeastern, South/Southeastern, Midwest, and Western United States, each designed to optimize pavement performance under local conditions.

### 5.2.1 Regional Influences on Asphalt Binder Specifications

The selection and modification of asphalt binders are strongly dictated by regional factors, including climate, traffic loads, and past performance experiences. Each state's DOT specifications are tailored to optimize the performance of pavement materials under the specific environmental and operational conditions they face. For example, regions that experience extreme temperature fluctuations—such as cold winters and hot summers—require binders that offer both superior resistance to rutting in high temperatures and cracking in low temperatures. Conversely, areas characterized by heavy traffic volumes, particularly from large vehicles, demand binders that are engineered for enhanced durability, stress resistance, and long-term resilience under constant load.

These regional requirements not only shape the choice of modified binders but also highlight the potential for expanding the use of innovative materials such as RAP and RAS. As with modified binders, these materials must be selected and optimized based on the unique environmental and traffic conditions of each region to ensure their effectiveness. By tailoring the specifications for both traditional and innovative materials, DOTs can meet local performance goals while simultaneously pursuing sustainable, cost-effective solutions for long-lasting pavement infrastructure.

#### 5.2.1.1 Northeastern United States

The Northeastern region of the U.S. is characterized by harsh winters, significant freeze-thaw cycles, and high precipitation levels. These factors necessitate the use of asphalt binders with superior thermal cracking resistance and durability.

- Common Specifications: Chapter 3 data indicates that states such as New York, Pennsylvania, and Massachusetts frequently specify PG 64S-22 for standard applications. For higher performance requirements, PG 64E-22 modified with SBS polymer is utilized, providing enhanced elasticity and resistance to deformation. Additionally, New York and Maine incorporate crumb rubber-modified binders (e.g., PG 58-28 CR) to improve the flexibility and longevity of pavements under extreme temperature conditions.

- Key Applications: These modified binders are often employed in high-stress areas such as urban roads, highways, and bridges, where long-term performance and reduced maintenance are critical. The use of SBS and crumb rubber modifications specifically addresses issues related to low-temperature cracking, a common challenge in this region.

#### 5.2.1.2 South/Southeastern United States

The South/Southeastern U.S. faces a different set of challenges, including high temperatures, humidity, and heavy rainfall, which can lead to significant rutting and moisture damage if not properly managed.

- Common Specifications: In this region, Chapter 3 data highlights that DOTs such as those in Florida, Louisiana, and Georgia frequently specify PG 76-22 ARB, a binder that includes ground tire rubber (GTR) for enhanced flexibility and rutting resistance. Alabama and Georgia use a range of binders from PG 58-22 for general applications to PG 76-22 for high-temperature conditions. The inclusion of modifiers like SBS and crumb rubber is crucial for maintaining pavement integrity under the intense heat and heavy traffic typical of this region.

- Key Applications: These binders are primarily used in areas prone to rutting, such as interstate highways, urban roads, and heavy-traffic corridors. The modified binders offer improved performance in both high-temperature stability and moisture resistance, making them essential for the long-term durability of pavements in this region.

#### 5.2.1.3 Midwest United States

The Midwest is known for its broad temperature range, from frigid winters to hot summers, requiring binders that can withstand thermal stresses and maintain performance across seasons.

- Common Specifications: According to Chapter 3 data, states like Illinois, Indiana, and Minnesota often use PG 64-22 and PG 70-28, with modifications such as SBS or SBR to enhance resistance to thermal cracking and rutting. Missouri DOT specifies PG 64-22 for general paving applications and PG 70-22 for areas requiring higher temperature resistance. Additionally, binders like PG 58-28 Modified are used in high-stress applications, where enhanced elasticity and durability are critical.

- Key Applications: These binders are commonly used in regional highways, arterial roads, and other critical infrastructure where the balance between flexibility in cold conditions and stiffness in hot conditions is vital. The inclusion of polymer modifications ensures that the pavements can resist cracking and rutting, even under the region's extreme weather conditions.

#### 5.2.1.4 Western United States

The Western U.S. encompasses a wide range of climates, from the cold, wet conditions of the Pacific Northwest to the hot, arid environments of the Southwest. As a result, binder specifications in this region are diverse and tailored to local needs.

- Common Specifications: For example, Chapter 3 data shows that Alaska uses PG 52-28, a binder suitable for its cold climate, while California and Nevada employ modified binders such as PG 76-22, designed for high temperatures and heavy traffic. In Nevada, rubber-modified binders like PG 64-28NVTR and PG 76-22NVTR are specified for their superior performance in extreme temperatures, preventing rutting and cracking. Arizona uses a range of binders, including PG 70-22 with crumb rubber and polymer modifications, to address the challenges posed by high heat and heavy traffic loads.

- Key Applications: In Alaska, binders like PG 52-28 are used in general paving applications where cold weather resilience is critical. Meanwhile, in California and Arizona, the focus is on preventing rutting and thermal cracking under high temperatures and heavy traffic, especially in major highways and urban areas. Rubber-modified binders are increasingly used in these states for their enhanced performance characteristics, especially in hot climates.

### 5.2.2 Analysis of DOT Specification Variations

The variation in DOT specifications across these regions reflects the need for region-specific solutions to address local climatic and traffic conditions. Chapter 3 data underscores that while some binders, such as PG 64-22, are commonly used across multiple regions, their modifications differ significantly to meet regional demands. For example:

Thermal Stress Management: In cold regions like the Northeastern and Midwest U.S., binder modifications focus on reducing thermal cracking, with polymers like SBS providing the necessary flexibility. Conversely, in the South and Southwest, the emphasis is on rutting resistance, with rubber modifications offering enhanced performance under high temperatures.

Traffic Load Considerations: High-traffic areas, regardless of region, require binders that can withstand repeated loading without deformation. States in the South and West often specify high-performance binders like PG 76-22 with polymer and rubber modifications, while Northeastern and Midwestern states may use a combination of high and low-temperature grades to balance performance across seasonal variations.

Environmental and Regulatory Compliance: Environmental considerations, such as the inclusion of recycled materials, also play a significant role in binder specification. For instance, many states have incorporated crumb rubber or other recycled materials into their binders to meet sustainability goals, as seen in the use of PG 76-22 ARB in Florida and Louisiana.

All in all, The DOT specifications for asphalt binder modifications across the United States are a testament to the regional diversity in climate, traffic demands, and environmental challenges. The data from Chapter 3 reveals that Northeastern states emphasize thermal cracking resistance, while the South/Southeastern states focus on rutting resistance and moisture management. The Midwest balances between thermal flexibility and high-temperature performance, and the Western states employ a wide range of modifications to address both hot and cold extremes.

Understanding these regional specifications is critical for developing tailored solutions that not only meet local performance requirements but also extend the lifespan of pavements, reduce maintenance costs, and enhance safety. As binder technology continues to evolve, it is likely that DOT specifications will increasingly integrate advanced materials and sustainability considerations, further optimizing pavement performance across the diverse landscapes of the United States.

## 5.3 Assessment of LTPP Database Coverage on Modified Binders

The LTPP database is a comprehensive resource that has amassed substantial data on pavement performance across North America since its inception. It contains detailed information on various pavement materials, structures, and their behavior under different environmental and traffic conditions. However, while the database provides significant value for research and decision-making, there are notable limitations in its coverage of modified asphalt binders.

Although the database includes data on modified binders, the extent and consistency of this information are not as thorough as might be required for a complete evaluation of their performance. Key gaps include insufficient data on the long-term behavior of modified binders in various climatic regions and under different traffic loads. Additionally, there is a lack of standardized reporting on the use of modified binders, leading to inconsistencies in data quality and comparability across different pavement sections.

This assessment highlights both the strengths and weaknesses of the LTPP database when it comes to modified binders. While it serves as a valuable starting point for understanding their impact on pavement performance, the limited and sometimes fragmented nature of the available data constrains the depth of analysis that can be performed. These gaps point to the need for enhanced data collection practices and expanded research efforts to improve the understanding of modified binders’ long-term performance.

Furthermore, expanding the scope of the database to include other innovative materials such as RAP and RAS could provide a more comprehensive understanding of their role in sustainable pavement performance. By broadening the database to better encompass a range of emerging materials, future research will be better equipped to evaluate the effectiveness of innovative paving solutions, thus advancing the field of pavement engineering.

### 5.3.1 Data Sources for Modified Binders

The LTPP database provides two primary methods for obtaining information on modified binders: the SDR file and the ARMAD. The SDR file contains detailed records of materials used in various pavement sections, including asphalt binder types, physical and chemical properties, and specific application areas, offering a historical perspective crucial for understanding long-term performance trends. ARMAD, on the other hand, provides a streamlined, pre-processed dataset focused on material, including critical information on binder types, formulations, and modifications, making it particularly useful for comparative studies, trend analysis, and the development of predictive models related to mixture performance.

### 5.3.2 Coverage and Limitations

While the LTPP database contains data on binders, its coverage is not comprehensive. As analyzed in Chapter 4, only a limited number of sections within the LTPP database involve the use of modified binders. The database does identify sections with modifiers such as SBS polymer, crumb rubber, and other additives, but these are relatively scarce compared to the total number of pavement sections cataloged. Tables in the document highlight specific sections utilizing modified binders, emphasizing the limited scope of available data for analysis.

The Inventory File within the SDR method provides a more detailed breakdown of the asphalt binders used in different sections, including their grades, sources, and specific properties. However, the data is often incomplete or lacks sufficient detail, particularly concerning modified binders. This data gap poses significant challenges for researchers attempting to evaluate the long-term performance and effectiveness of these materials.

Additionally, sections classified as 6C or 7C refer to construction numbers associated with years following the initial project, but all binder information pertains only to the first construction. This means that even if modified binders were used for overlaying in these later sections, the binder information linked to that specific construction number is inaccessible. This further complicates the ability to analyze the impact of modified binders in subsequent pavement projects.

### 5.3.3 Implications for Research and Pavement Performance

The gaps in the LTPP database regarding modified binders limit the ability to conduct comprehensive analyses and draw reliable conclusions about their performance. Without sufficient data on the use and performance of modified binders, it becomes difficult to develop robust predictive models or to fully understand the benefits and drawbacks of these materials under various conditions.

Moreover, the limited data hampers efforts to evaluate the long-term cost-effectiveness and durability of modified binders, which are critical factors for transportation agencies when making decisions about pavement materials. As a result, there is a need for improved data collection practices within the LTPP framework to ensure that future research can better address these knowledge gaps and support the optimization of pavement materials.

The assessment of LTPP database coverage on modified binders reveals that while valuable data is available, it is not comprehensive enough to fully support the analysis and optimization of these materials. The limited coverage restricts the ability to evaluate the long-term performance of modified binders, which is essential for advancing pavement technology. To overcome these challenges, further efforts to standardize data collection and enhance the comprehensiveness of the LTPP database are necessary. Such improvements will enable more effective research and contribute to the development of more durable, cost-effective, and sustainable pavement solutions.

### 5.3.4 Identifying Gaps in Data: Challenges in Evaluating Modified Binders

The LTPP database, encompassing 2,581 pavement sections, faces considerable challenges in evaluating modified binders due to notable data gaps. Out of these sections, only 38 provide detailed information on modified binders, representing a mere 1.47% of the total. The data available for analyzing modified binder is sparse and uneven, making it difficult to conduct thorough assessments.

Among the available sections, different modifiers such as lime, synthetic latex, block copolymer, and reclaimed rubber are documented, but their usage is minimal. For instance, Table 4.5 of the report lists various modifiers found in the LTPP database, but the number of sections using these modifiers remains limited. Additionally, Table 4.7 identifies the specific pavement sections utilizing these modifiers across different states. For example, lime (modifier code 2) is used in several sections across Colorado, Georgia, Montana, Texas, Utah, and Wyoming. Similarly, synthetic latex (modifier code 8) and block copolymer (modifier code 9) are found in a few sections in states such as Arizona, Tennessee, and Utah. However, these sections collectively represent only a small subset of the total LTPP database, highlighting the limited scope for comprehensive analysis.

A significant challenge in evaluating modified binders is the lack of information on the PG of the binders in the LTPP database. Despite the importance of PG grading in determining binder suitability, no PG data is provided for any section in the database. Additionally, even if we attempt to estimate the PG grades based on binder viscosity, the data is insufficient. As shown in Table 4.4, which details the “INV_PMA_ASPHALT” table, critical parameters such as original viscosity at 140°F and 275°F are only available for 66.30% and 56.59% of sections, respectively. The overall availability of relevant data across all parameters averages only 27.76%. This insufficiency prevents any reliable estimation of PG grades, further complicating efforts to evaluate binder performance.

In conclusion, the LTPP database suffers from significant data gaps, particularly regarding modified and highly modified binders. The limited number of sections with detailed information, combined with the absence of PG grade data and the inadequacy of viscosity data, presents substantial obstacles to advancing pavement research. These gaps, as highlighted in Tables 4.4, 4.5, and 4.7, underscore the need for improved data collection methodologies to better capture the performance characteristics of these materials. Addressing these shortcomings is essential for enabling more robust analyses and supporting the broader adoption of innovative pavement materials.

# Chapter 6. Conclusions and Recommendations

## 6.1 Conclusion

This study has provided a comprehensive analysis of the LTPP database and state specifications, with a particular focus on the performance of innovative paving materials such as modified binders. Despite the extensive data housed in the LTPP database, significant gaps remain that limit the ability to fully evaluate the use and long-term performance of these materials.

One of the key findings is that while a survey indicates that 21 agencies are using modified binders, this usage is not fully reflected in the LTPP database for the current project. Additionally, although all DOTs specify different types of modified binders in their state specifications, these are often not documented within the LTPP database, creating a significant gap in the available data.

Furthermore, modified binders should be seen as representatives of a broader range of innovative materials, including RAP and RAS, which are increasingly adopted in pavement engineering. Expanding research to include these materials would provide a more holistic understanding of their potential benefits for improving pavement performance and sustainability.

The evaluation is also complicated by the classification of sections under codes 6C and 7C, which refer to construction numbers associated with years following the initial project. However, all binder information in the LTPP database pertains only to the first construction phase. This means that even if modified binders were used in overlays in these later sections, the binder-specific information for those subsequent constructions remains inaccessible. The absence of data on later construction phases further hinders the ability to assess the long-term impact of modified binders.

In addition, a lack of collaboration between PMS and the LTPP database has been identified as a critical challenge. Improved coordination between state-level PMS data collection efforts and the LTPP would ensure that comprehensive and consistent data on modified binders and other innovative materials are captured. This would enable a more complete analysis of material performance and support more effective predictive modeling.

In conclusion, addressing these data gaps—both in the coverage of subsequent construction phases and in fostering stronger collaboration between PMS and LTPP—will be essential to unlocking the full potential of the LTPP database. By viewing modified binders as a gateway to exploring broader innovative materials, and by improving data-sharing practices, the industry can advance toward more durable, sustainable, and cost-effective pavement infrastructure.

## 6.2 Recommendations

To address the identified limitations and enhance the utility of the LTPP database, the following recommendations are proposed:

- Comprehensive Data Inclusion: The LTPP database should be expanded to capture detailed information on all modified binders used across various phases of pavement projects, including overlays and subsequent construction activities. This will enhance the depth and scope of data available for performance evaluation.

- Standardized Documentation: A uniform system for documenting the use of modified binders should be implemented across all state agencies. Consistent reporting will ensure that the data in the LTPP database is complete, comparable, and reliable across different regions, improving performance assessments.

- Integration of Survey Data: Data from state and agency surveys on the use of modified binders should be incorporated into the LTPP database. This will provide a more accurate and current reflection of practices being implemented across various states.

- Expansion of Data Collection: The LTPP database should expand its collection efforts to include more detailed records of binder properties, modifications, and performance grades, particularly for sections categorized under codes like 6C and 7C. This will improve the tracking and evaluation of modified binders over time.

- Ongoing Research and Expansion to Innovative Materials: In addition to filling the data gaps on modified binders, future research should extend to other innovative materials such as RAP and RAS. Continuous research should focus on understanding the long-term performance of these materials and developing predictive models that incorporate expanded data for more accurate pavement performance predictions.

By implementing these recommendations, the LTPP database can evolve into a more powerful resource for advancing pavement technology, leading to the development of more durable, cost-effective, and sustainable infrastructure solutions.

# References

Alabama Department of Transportation. General Application Special Provision (Asphalt Pavement). September 8, 2022. Effective May 1, 2023.

Alabama Department of Transportation. Standard Specifications for Highway Construction. 2022.

Alaska Department of Transportation and Public Facilities. Alaska Flexible Pavement Design Manual. September 2004.

Alaska Department of Transportation and Public Facilities. Asphalt Pavement Inspector’s Manual. March 2022.

Alaska Department of Transportation and Public Facilities. Asphalt Surface Treatment Guide. October 2017.

Almusawi, Ali, Sarmad Shoman, and Andrei P. Lupanov. "Assessment of the effectiveness and the initial cost efficiency of hot recycled asphalt using polymer modified bitumen." Case Studies in Construction Materials 18 (2023): e02145.

Arizona Department of Transportation. Standard Specifications for Road and Bridge Construction. 2021.

Arkansas State Highway and Transportation Department. Standard Specifications for Highway Construction. 2014.

Bagui, Swapan Kumar, and Ambarish Ghosh. "Economic And Financial Analysis For Polymer Modified Bitumen." Malaysian Journal of Civil Engineering 24, no. 1 (2012).

California Department of Transportation. Standard Specifications. 2023 Edition.

Celaya, B. J., Haddock, J. E. (2006). Investigation of Coarse Aggregate Strength for Use in Stone Matrix Asphalt. Final Report. FHWA/IN/JT2P-2006/4. Indiana Department of Transportation.

Colorado Department of Transportation. Standard Specifications for Road and Bridge Construction. 2023.

Connecticut Department of Transportation. Standard Specifications for Roads, Bridges, Facilities and Incidental Construction. Form 819, 2024.

Delaware Department of Transportation. Standard Specification for Road and Bridge Construction. January 2024.

District of Columbia Department of Transportation. Standard Specifications for Highways and Structures. 2013.

Federal Highway Administration. Development and Use of the LTPP Analysis-Ready Materials Dataset. FHWA-HRT-23-111, December 2023.

Federal Highway Administration. Guide to Select Long-Term Pavement Performance Traffic Data for Multiple Uses. FHWA-HRT-24-062, March 2024.

Federal Highway Administration. LTPP Inventory Data Collection Guide. FHWA-RD-05-083, July 2005.

Florida Department of Transportation. Standard Specifications for Road and Bridge Construction. FY 2024-25.

Georgia Department of Transportation. Standard Specifications Construction of Transportation Systems. 2021 Edition.

Habbouche, Jhony, Elie Y. Hajj, Peter E. Sebaaly, and Murugaiyah Piratheepan. "A critical review of high polymer-modified asphalt binders and mixtures." International Journal of Pavement Engineering 21, no. 6 (2020): 686-702.

Habbouche, Jhony, Elie Y. Hajj, Peter E. Sebaaly, and Murugaiyah Piratheepan. "A critical review of high polymer-modified asphalt binders and mixtures." International Journal of Pavement Engineering 21, no. 6 (2020): 686-702.

Habbouche, Jhony, Ilker Boz, Brian K. Diefenderfer, Bryan C. Smith, and Sayed Hamidullah Adel. "State of the practice for high polymer-modified asphalt binders and mixtures." Transportation Research Record 2675, no. 7 (2021): 235-247.

Hawaii Department of Transportation. Section 404 - Slurry Seal. 2005.

Hawaii Department of Transportation. Section 407 - Tack Coat. 2005.

Hawaii Department of Transportation. Section 702 - Bituminous Materials. 2005.

Idaho Transportation Department. Standard Specifications for Highway Construction. 2023.

Illinois Department of Transportation. Standard Specifications for Road and Bridge Construction. Adopted January 1, 2022.

Illinois Department of Transportation. Supplemental Specifications and Recurring Special Provisions. Adopted January 1, 2024.

Indiana Department of Transportation. Standard Specifications. 2024.

Iowa Department of Transportation. Standard Specifications for Highway and Bridge Construction. Series 2023.

Kansas Department of Transportation. Division 1200 - Asphalt Materials. 2015.

Kansas Department of Transportation. Division 2600 - Materials Certifications. 2015.

Kansas Department of Transportation. Division 600 - Flexible Pavement. 2015.

Kaya, O., Ceylan, H., and Moore, B. (2020), Statistics and Artificial Intelligence-Based Pavement Performance and Remaining Service Life Prediction Models for Flexible and Composite Pavement Systems. Transportation Research Record. 2674(10), 448-460.

Kentucky Transportation Cabinet. Standard Specifications for Road and Bridge Construction. Edition of 2019. Approved for June 1, 2019.

Li, Ruoyu, Feipeng Xiao, Serji Amirkhanian, Zhanping You, and Jia Huang. "Developments of nano materials and technologies on asphalt materials–A review." Construction and Building Materials 143 (2017): 633-648.

Lin, Peng, Chuanqi Yan, Weidong Huang, Yi Li, Lu Zhou, Naipeng Tang, Feipeng Xiao, Yi Zhang, and Quan Lv. "Rheological, chemical and aging characteristics of high content polymer modified asphalt." Construction and Building Materials 207 (2019): 616-629.

Liu, J. (2010). Evaluation of Warm Mix Asphalt for Alaska Conditions. Final Report. Alaska Department of Transportation Research, Development, and Technology Transfer. FHWA-AK-RD-12-12.

Liu. J, and Liu, J. (2019). Laboratory and Field Evaluation of Modified Asphalt Binders and Mixes for Alaskan Pavements. Final Report. Alaska Department of Transportation & Public Facilities Statewide Research Office. FHWA-AK-RD-4000(176).

Louisiana Department of Transportation and Development. Standard Specifications for Roads and Bridges. 2016 Edition. Baton Rouge, Louisiana: Louisiana Department of Transportation and Development, 2016.

Maine Department of Transportation. Standard Specification for Roads and Bridges. March 2020.

Marcelino, P., Antunes, M. de L., Fortunato, E., and Comes, M. C. (2021). Machine learning approach for pavement performance prediction. International Journal of Pavement Engineering. 22(3): 341-354.

Maryland Department of Transportation State Highway Administration. Standard Specifications for Construction and Materials. July 2022.

Massachusetts Department of Transportation. Standard Specifications for Highways and Bridges. 2021 Edition.

Michigan Department of Transportation. Standard Specifications for Construction. 2020 Edition.

Minnesota Department of Transportation. Standard Specifications for Construction. 2020 Edition, Volume 1.

Minnesota Department of Transportation. Standard Specifications for Construction. 2020 Edition, Volume 2.

Minnesota Department of Transportation. Supplemental Specifications to the 2020 Standard Specifications for Construction. September 2022.

Mississippi Department of Transportation. Standard Specifications for Road and Bridge Construction. 2017 Edition. Approved and Adopted by the Mississippi Transportation Commission, Jackson, November 8, 2016.

Missouri Department of Transportation. Standard Specifications for Highway Construction. 2021 Edition.

Montana Department of Transportation. Standard Specifications for Road and Bridge Construction. 2020 Edition. Effective September 9, 2021.

Nebraska Department of Transportation. Standard Specifications for Highway Construction. 2017 Edition.

Nevada Department of Transportation. Standard Specifications for Road and Bridge Construction. 2014 Edition.

New Hampshire Department of Transportation. Amendment to Section 401 – Plant Mix Pavement – General. June 18, 2024,​.

New Hampshire Department of Transportation. Amendment to Section 403 – Hot Bituminous Pavement. July 1, 2021.

New Hampshire Department of Transportation. Amendment to Section 410 – Bituminous Surface Treatment. July 6, 2018.

New Hampshire Department of Transportation. Amendment to Section 411 – Plant Mix Surface Treatment. January 11, 2024.

New Hampshire Department of Transportation. Amendment to Section 417 – Cold Planning of Bituminous Surfaces. April 2, 2018.

New Hampshire Department of Transportation. Amendment to Section 702 – Bituminous Materials. January 11, 2024.

New Hampshire Department of Transportation. Standard Specifications for Road and Bridge Construction. 2016 Edition.

New Jersey Department of Transportation. Standard Specifications for Road and Bridge Construction. 2019 Edition.

New Mexico Department of Transportation. 2019 Standard Drawings for Highway and Bridge Construction. Updated October 2023.

New Mexico Department of Transportation. Standard Specifications for Highway and Bridge Construction. 2019 Edition.

New York State Department of Transportation. Standard Specifications (Vol 1) Section 100. September 1, 2024.

New York State Department of Transportation. Standard Specifications (Vol 2) Section 200-599. September 1, 2024.

New York State Department of Transportation. Standard Specifications (Vol 3) Section 600. September 1, 2024.

New York State Department of Transportation. Standard Specifications (Vol 4) Section 700. September 1, 2024.

North Carolina Department of Transportation. Standard Specifications for Roads and Structures. January 2018 Edition.

North Dakota Department of Transportation. Standard Specifications for Road and Bridge Construction. Adopted July 1, 2024.

Ohio Department of Transportation. Construction and Material Specifications. January 1. 2023 Edition.

Oklahoma Department of Transportation. Standard Specifications for Highway Construction. 2019 Edition.

Oregon Department of Transportation. Standard Specifications for Construction. 2024 Edition.

Pennsylvania Department of Transportation. Specifications. PUB 408/2020, updated October 6, 2023.

Rhode Island Department of Transportation. Standard Specifications for Road & Bridge Construction. February 2024 Edition.

Ruth, P., Majidifard, H., Beckemeyer, P., Meister, R., and Butter, W. C. (2023). Post-Production Evaluation and Field Monitoring of Ground Tire Rubber and Post-Consumer Recycled Plastic Modified Asphalt Mixtures. Presentation of Transportation Research Board.

Song, Y., Wang, Y. D., Hu, X., and Liu, J. (2022). An Efficient and Explainable Ensemble Learning Model for Asphalt Pavement Condition Prediction Based on LTPP Dataset. IEEE Transactions on Intelligent Transportation Systems. 23(11).

South Carolina Department of Transportation. Standard Specifications for Highway Construction. 2007 Edition.

South Dakota Department of Transportation. Standard Specifications for Roads and Bridges. 2015 Edition. Supplemental Specifications September 7, 2022.

Sulyman, Mohamed, Maciej Sienkiewicz, and Jozef Haponiuk. "Asphalt pavement material improvement: a review." International journal of environmental science and development 5, no. 5 (2014): 444.

Tennessee Department of Transportation. Standard Specifications for Road and Bridge Construction. January 2021 Edition.

Texas Department of Transportation. Standard Specifications for Construction and Maintenance of Highways, Streets, and Bridges. November 1, 2014.

Utah Department of Transportation. Standard Specifications for Road and Bridge Construction. 2025 Edition. Approved January 1, 2025.

Vermont Agency of Transportation. Standard Specifications for Construction. 2024 Edition. Adopted June 2023.

Virginia Department of Transportation. 2022 Supplement to the 2020 Road and Bridge Specifications. December 31, 2021.

Virginia Department of Transportation. Road and Bridge Specifications. 2020 Edition.

Wang, Yuhong, Dan Chong, and Yong Wen. "Quality verification of polymer-modified asphalt binder used in hot-mix asphalt pavement construction." Construction and Building Materials 150 (2017): 157-166.

Washington State Department of Transportation. Standard Specifications for Road, Bridge, and Municipal Construction. M 41-10, 2024 Edition.

West Virginia Department of Transportation. 2024 Supplemental Specifications to the 2023 Edition of Standard Specifications for Roads and Bridges.

West Virginia Department of Transportation. Standard Specifications Roads and Bridges. 2023 Edition.

Wisconsin Department of Transportation. 2024 Supplemental Specifications to the 2024 Edition of Standard Specifications for Road and Structure Construction.

Wisconsin Department of Transportation. Standard Specifications for Road and Structure Construction. 2024 Edition.

Wu, Wangjie, Maria Chiara Cavalli, Wei Jiang, and Nicole Kringos. "Differing perspectives on the use of high-content SBS polymer-modified bitumen." Construction and Building Materials 411 (2024): 134433.

Wyoming Department of Transportation. Standard Specifications for Road and Bridge Construction. 2021 Edition. Adopted by the Transportation Commission of Wyoming, August 20, 2020.

Yang, Jun, and Susan Tighe. "A review of advances of nanotechnology in asphalt mixtures." Procedia-Social and Behavioral Sciences 96 (2013): 1269-1276.

Yildirim, Yetkin. "Polymer modified asphalt binders." Construction and building materials 21, no. 1 (2007): 66-72.

Zhu, Jiqing, Xiaohu Lu, Michael Langfjell, and Anders Gudmarsson. "Quantitative relationship of fundamental rheological properties of bitumen with the empirical Ring and Ball softening point." Road Materials and Pavement Design 22, no. sup1 (2021): S345-S364.

Ziari, H., Sobhani, J., Ayoubinejad, J., and Hartmann, T. (2015). Prediction of IRI in Short and Long Terms for Flexible Pavements: ANN and GMDH Methods. International Journal of Pavement Engineering. 17(9): 776-788.